6. IMPACT RESISTANCE OF SOILS, CONCRETE AND STEEL – CONCRETE STRUCTURES

In the preceding sections the penetration and perforation of metallic plates with kinetic energy penetrators has been discussed and the dominant and most frequently occurring failure mechanisms have been identified. When targets made of a non-metallic material are struck by projectiles the penetration processes and failure mechanisms involved are often very different.

The penetration of soils and terrestrial media has been of long standing interest to impact engineers. Young [6] gives a brief account of the historical development of the various empirical equations that are still used today to predict the depth of penetration, Z, achieved by a projectile striking a semi-infinite body. These equations are

Robins – Euler (1742):

Z=mpV022a0;                                    (68)

Poncelet (1830):

Z=mp2a2ln1+a2V02a0 ;                            (69)

Resel (1895):

Z=mpa2ln1+a2V0a1  ;                           (70)

Petry (1910):

Z=WApKlog101+V02215,000.                   (71)

In Eqns (68) – (71) a0,a1,a2 are constants from the empirical polynomial relating the impact force to impact velocity,

F=a0+a1V0+a2V02+...+anV0n.              (72)

In Eqn (71) Z is in ft, V0 is in ft/s, W (projectile weight) is in lb, Ap(cross-sectional area of projectile) is in square inches and K is a constant dependent on the target material.

Young [6] carried out a number of experiments to determine the effects of various parameters, including projectile nose shape, projectile mass and area and impact velocity on the penetration distance. The results were used to propose an empirical prediction of penetration distance,

Z=0,53SNWA12ln1+2V02´10−5  for V0<200 ôóò/ñ;    (73a)

Z=0,0031SNWA12V0−100   for  V0>200 ôóò/ñ.       (73b)

In these equations S is a soil constant (examples of which are given in [6]) and N is a nose performance coefficient (between 0.56 for a flat-faced projectile and 1.32 for a shallow cone). All the other parameters are as defined, and in the same units, as for the Petry equation [Eqn (71)]. It is interesting to note that a bi-functional relationship was also proposed by Jowett [82] for the impact of finite thickness steel plates. This relationship [Eqn (15)] related perforation energy to relative plate thickness and the function to be used depended on the relative thickness of the plate tested.

Various analytical models have been developed to predict the depth of penetration and the forces experienced by the projectile during penetration into semi-infinite targets (for example [155 – 163]), and a number of experimental studies have been carried out to investigate their authenticity [164, 165]. The application of numerical methods to the problem are discussed in [147, 160, 166, 167]. In addition to these Backman and Goldsmith [2] devote a section of their paper to the penetration of semi-infinite bodies.

The projectile impact on materials such as wood [168, 169], ceramics [170 – 173] and GRP or CFRP composites [174 – 180] has also received attention from a number of researchers.

A material that is of particular interest to impact engineers is concrete. Where weight and space are not factors that need to be kept to a minimum, concrete in the form of walls or barriers is often used. One very important example of an industry that relies heavily on the impact resistance of concrete is the nuclear industry which requires the walls of certain structures to be able to withstand impact by accidentally generated missiles [181]. Although there have been attempts at modelling the impact of semi-infinite concrete structures with projectiles (for example [182, 183]), this section in common with the previous sections on the impact of metallic targets, is only concerned with the impact of finite thickness concrete targets. Once again the emphasis is placed on work highlighting the penetration and perforation processes involved when a target is struck by a projectile travelling at near its ballistic limit.

A review of the progress made in understanding the mechanics of projectile impact on concrete structures has been made by Kennedy [184]. The processes of penetration and perforation of concrete is very different from that of metal and is summarized in Fig. 71. Once the initial projectile velocity is large enough to damage the concrete, pieces of it spall (are ejected) from the impact face of the target forming a crater that extends over a considerably greater area than the impact area. As the impact velocity is increased the projectile penetrates to depths greater than that of the spall crater, producing a hole in the concrete with a diameter only slightly greater than the projectile diameter. Further increase in the initial projectile velocity results in cracking and then scabbing (ejection) of concrete from the rear surface. The zone of scabbing is generally more extensive but less deep than that of the front spall crater. As these ejected concrete pieces (from the rear surface) could themselves constitute a hazard it is often necessary to define two thicknesses when designing a protective shield: the minimum thickness to prevent perforation, p, and the minimum thickness to prevent scabbing, s. Once scabbing has begun, the depth of penetration increases rapidly with increasing impact velocity leading eventually to perforation of the target as the penetration hole extends through to the scabbing crater. As in the penetration of metal plates, for certain target geometries global response will play an important role in the impact resisting capabilities of the target [184].

Analysis of steel reinforced concrete is extremely difficult as the dominant energy absorbing mechanisms and failure modes of the constitutive elements are different and interact with each other. Consequently the majority of investigations into the penetration and perforation of concrete targets have been of an empirical nature. In most cases the empirical predictions of penetration into semi-infinite targets have been adapted to predict thicknesses required to prevent perforation by a projectile with a given velocity for finite thickness targets. The study of penetration of projectiles into concrete structures has been heavily influenced by the interests of military establishments. As Kennedy [184] points out, the majority of published work has been concerned with deriving empirical formulae for the normal impact of concrete structures by non-deformable projectiles, this being assumed to be the most destructive combination for a given projectile mass and velocity. These empirical formulae were obtained prior to 1946, with the majority of the subsequent work being carried out by the military and thus being classified. The most commonly used formulae are listed below:

1. Modified Petry formula [see Eqn (71)]

p=2x;                                    (74a)

s=2,2x,                                 (74b)

where

x=12KpWAplog101+V02215,000,                  (74c)

where p, s and x are in inches and V0 is in ft/s. WAp is the weight of the missile per unit projected area in lb/ft2. There are two types of modified Petry formula. In the modified Petry I formula Kp=0.00799 for massive concrete, 0.00426 for normal reinforced concrete and 0.00284 for specially reinforced concrete and is independent of the concrete strength. In modified Petry II, Kpis a function of the concrete strength (see Fig. 72).

2. U.S. Army Corps of Engineers formula (ACE)

pdp=1,32+1,24xdp   for   3≤pdp≤18;               (75a)

sdp=2,12+1,36xdp   for   3≤sdp≤18,              (75b)

where

xdp=282Ddp0,215fc12V010001,5+0,5.                   (75c)

Here, D is the calibre density of the projectile (lb/in2), dp is the projectile diameter (in), fc is the ultimate compressive strength of the concrete (lb/in2).

3. Modified National Defence Research Committee formula (NDRC)

xd is obtained from

G(x,dp)=KpNdp0.20DV010001.18

and

G(x,dp)=x2dp2forxdp≤2.0,

G(x,dp)=xdp−1forxdp³2.0.                 (76)

Here, N is a missile nose shape factor: N = 0.72 for flat nosed missiles, 0.84 for blunt nosed missiles, 1.00 for spherical missiles and 1.14 for sharp nosed missiles. The concrete strength is given by K = 180/fc. p/d and s/d are then calculated from Eqns (75).

4. Amman and Whitney formula (for V0 > 1000 ft/s)

xdp=282NDdp0,2fc12V010001,8                          (77)

and Eqns (75) are used to evaluate p and s

5. Ballistic Research Laboratory (BRL) formula

pdp=427Ddp0,2fc12V010001,33;                        (78a)

s=2p.                                                  (78b)

All these formulae are applicable to situations that lie within the following parameters (unless otherwise stated):

h0dp³3;dp≤16in;0.2≤D≤0.8lbin3;3≤pdp≤18;500≤V0≤3000fts;3≤sdp≤18.

As with all empirical formulae those stated here are only valid when the above conditions are met and any deviation from these is liable to render the formulae highly inaccurate. The two restrictions most likely to be violated in non-military impact situations are those of target thickness – projectile diameter ratio (h0d) and projectile velocity (V0).

The only one of the above empirical formulae to have a theoretical basis is the NDRC formula and it is probably because of this that it is the only one that can be successfully extrapolated beyond the conditions from which it was originally derived. By creating a parabolic fit between xdp = 0 and xdp = 3 to Eqn (76) the following expressions were derived [184]

pdp=3,19xdp−0,718xdp2  for  xdp≤1,35;            (79a)

sdp=7,91xdp−5,06xdp2   for   xdp≤0,65.          (79b)

xdp is obtained from Eqn (76). For larger xd ratios Eqns (75) are used.

The NDRC formula, because of its theoretical basis and ability to be extrapolated over a wide range of variables, is recommended for use by Kennedy [184]. Over the entire range of variables mentioned (missile diameters up to 16 in, calibre densities between 0.2 and 16 lb/in2 and missile velocities 100 – 3000 ft/s) the NDRC formula predicted the perforation and scabbing thicknesses to within ±20%. In these tests concrete reinforcement of 0.4 – 0.6% EWEF (Each-Way-Each-Face ratio of steel to concrete) was used. It was noted that all the empirical equations assume no projectile deformation or target deformation away from the area of impact.

Kennedy [184] also describes how the NDRC formula can be used to describe the force – time history of the impact process as well as discussing qualitatively the effects of missile deformation, target inertial weight and global target response on the penetration process.

Sliter [181] collected test data on the impact of concrete targets from a number of different sources and used them to assess the validity of the older empirical formulae. Like Kennedy [184], Sliter came to the conclusion that the NDRC formula is the most suitable for the widest range of impact parameters. Two parameters that are not incorporated in the NDRC formula are the relative aggregate size (dp/C) and the amount of reinforcement. Sliter [181] investigated the effect that these parameters have on the impact process and found that there was only a weak dependence of penetration depth on both these factors, over the range 0.5 – 50 for the former and 0.3 – 1.5% for the latter (where the percentages refer to the areal percentage of reinforcement in both directions). There were no test data available for heavily reinforced targets most likely to be found in conventional reinforced concrete walls (1.5 – 3% each way).

Sliter [181] investigated the applicability of the NDRC formula to low velocity impacts (< 300 m/s). It was found that the penetration depth was predicted to within 25% by the NDRC formula provided that the depth of penetration was greater than 0.6dp which corresponded to an impact velocity of greater than 150 m/s for the test conditions that were analysed. When the penetration depth achieved by the projectile was less than 0.6dp the NDRC formula tended to over-predict the penetration depth. Sliter [181] also compared experimental data from a variety of sources with the predictions of equations and found that agreement between the two was poor for large dph0 ratios. This was attributed to the relatively large-area planar impact (all the tests involved flat-faced cylindrical projectiles) inducing scabbing from the tensile shock wave resulting from the compressive wave reflected from the back surface, while producing little penetration. It was concluded that the NDRC formula could not be used with confidence in impact situations with low xdp ratios or high dph0 ratios to predict the scabbing thickness. Two alternative empirical formulae were proposed for these situations which were derived from tests involving the thickness – diameter ratios of interest. These were the Bechtel formula,

s=15,5W0,4V00,5fcdp0,2                               (80)

and the Stone and Webster formula

s=WV02C13,                               (81)

in which C is a coefficient dependent on the h0dp ratio. The range of test parameters to which these equations can be applied are 3000 lb/in2 < fc< 4500 lb/in2 and 1.5 < h0dp < 3. These formulae were seen to be in reasonable agreement with experimental data.

For predicting perforation thickness, Sliter [181] found the following CEA/ADF formula to give the best agreement with the experimental data available

p=0,765fc−38Wdp12V034.                  (82)

In Eqn (82) the density of the concrete has been taken as 2500 kg/m3 and the reinforcement quantity as being between 0.8% and 1.5% each way. Sliter noted that reinforcement quantity is likely to have a substantial effect on the perforation thickness and therefore Eqn (82) should not be used on concrete structures with reinforcement quantities outside the range stated.

Perry et al. [185] discussed the factors influencing the response of fibre-reinforced concrete slabs to impact and noted that changing the amount of fibre reinforcement may change the mode of failure of the concrete with unreinforced concrete tending to fail by shear punching and steel-fibre reinforced concrete tending to fail by flexure and crushing of the concrete. In [186] the damaged specimens from these tests, along with damaged dome specimens from a series of impact tests carried out on reinforced concrete domes [187], were repaired using a variety of cementitious and epoxy resin formulations. The static strengths of the repaired structures were tested and the efficiency of the repairs was assessed. It was shown that when certain conditions were met it was possible to regain a large percentage of the original strengths of the structures using both types of repair material.

Barr et al. [188] report on preliminary impact tests on reinforced concrete structures. They reviewed past work on similar impact tests, ran a series of tests themselves and introduced a short finite difference code, SARCASTIC, intended as a vehicle for assessment of the different theoretical constitutive models for concrete. The results of the tests were compared with the modified NDRC formula (76) and the velocities for perforation compared with the CEA/ADF formula.

Vx2=1,7fcρc13dh2mp43,                         (83)

where ρc is the concrete density and h is the concrete thickness. The limits of applicability of Eqn (83) are 20 < V0 < 200 m/s, 0.3 < h/d < 4, 30 < fc < 45 MPa. It should be noted that the CEA/ADF formula does not contain a reinforcement quantity-dependent parameter.

Comparison with the modified NDRC formula showed an agreement within 30%, but comparisons with the CEA/ADF formula were not possible since the test parameters were outside the range of validity. The results of the computer runs were inconclusive indicating that further work needs to be done before the code can be used as a design tool.

Initial tests on the possibility of scaling showed promise, and this theme was followed up in a subsequent report [189]. In this report tests were described on models of 1/2 – 1/16 typical full size dimensions with reasonable agreement between the models and the prototype being found.

A common method employed to increase the impact resistance of concrete slabs is to attach front face and/or rear face cladding to the surfaces of the slab. This serves either to increase the ballistic limit of the structure or to reduce the required wall thickness to obtain a particular ballistic limit. The effect of reinforcing a concrete structure in this way has been studied by Barr et al. [190,191] who conclude that:

(i) The perforation energy of a barrier with impact face cladding is equal to the sum of the perforation energies of each of the components considered alone.

(ii) Rear face cladding behaves in a manner analogous to additional rear face bending reinforcement. Cladding and internal reinforcement are equivalent when the cross-sectional areas of reinforcement and plate and the elasto-plastic parameters of the steels are equal.

For reinforced (both internally and externally) target slabs, the following amendment to the CEA/ADF formula that incorporates a reinforcement parameter was proposed:

Vx2=1,7fcρc13dh2mp43r+0,3,                         (84)

where r, the bending reinforcement quantity in % EWEF (Each-Way-Each-Face), lies between 0 and 4%.

(iii) For concrete barriers with steel cladding on both impact and rear faces, the perforation energy for the composite is equal to the sum of the perforation energies of the front face cladding alone and that of the remainder of the barrier. Tests on blockwork barriers showed that these appear to have a perforation energy about 70% that of monolithic barrier of the same strength as the blocks themselves.

The residual velocity of a 25.4 mm diameter, 0.5 kg mass, ogival-nose projectile perforating 178 mm thick reinforced concrete slabs was shown to be disproportionately influenced by the unconfined compressive strength of the concrete by Hanchak et al. [192]. A three-fold increase in the unconfined compressive strength resulted in a decrease in the residual velocity of less than 20%. It was shown that the influence of a lateral restraining pressure on the concrete exerted by the surrounding mass served to decrease the influence of the unconfined compressive strength. It was also shown that the ballistic limit was insensitive to whether or not the projectile struck the reinforcing bars during penetration.

The response of steel – grout sandwich plates to projectile impact was investigated by Corbett and Reid [193]. It was shown that sandwich plates made up of two 1 mm thick steel skins separated by grout fillers with thicknesses ranging from 3 to 40 mm were not as efficient at withstanding projectile impact in terms of energy absorbed per areal density as monolithic steel plates for the impact conditions used in the test programme (a 12.7 mm diameter hemispherically-ended cylindrical projectile travelling at between 40 and 200 m/s). It was shown that the dominant energy absorbing components were the rear face skin and the grout filler, with the impact face skin absorbing relatively little energy. Two examples of impact damaged sandwich plates, one thin and one thick, are shown in Fig. 73. The plates have been dismantled to show the dominant deformation and failure mechanisms of the different plate components. It can be seen that for both of the plates the impact face steel skin is deformed less than the rear face skin, with the impact face skin of the thick plate showing signs of "reverse dishing", that is dishing in the opposite direction to the direction of impact. This is a result of frontal spalling of the grout filler. Figure 73(c) also shows a typical failure cone that is formed when moderately thick concrete or grout is subjected to projectile penetration.

In a similar set of tests Corbett et al. [194] investigated the resistance of steel – concrete sandwich tubes to penetration from hardened steel indenters. Concrete tubes were clad on their outer and inner diameters with 1 mm thick steel skins and subjected to local loading, quasi-static and dynamic. The tubes tested all had an inner diameter of 120 mm. Concrete filler thicknesses of 10, 20 and 38 mm were examined. As in the sandwich plate tests, loading was applied with a hemispherically-ended indenter. The performance of the sandwich tubes under this type of loading was compared with that of monolithic steel tubes tested in a companion paper [62], discussed in Section 2.5. It was found that, over the range of thicknesses tested, this type of sandwich construction required a filler thickness approximately five times greater than the thickness of monolithic steel tubes in order to be able to absorb the same amount of impact energy under similar loading conditions. It was shown in [193] and [194] that the impact resistance of steel – concrete and steel – grout sandwich structures were less sensitive to projectile mass and projectile nose shape than monolithic steel structures. In addition the resistance of the sandwich structures to projectile penetration was seen to be most effective when the rear face skin was undeformed, thus providing substantial support to the filling medium. It was therefore proposed that a sandwich structure that is effective at resisting projectile penetration would be one that was made up of a thick steel backing plate/shell that would absorb most of the energy and provide support to the filler and a bulky filler held in place by a relatively thin impact face skin. The latter components of the sandwich would protect the energy absorbing rear face skin from "unfavourable" impact conditions (such as sharp-faced, rapidly moving projectiles) by spreading the load and reducing the penetration velocity.

Gandeker et al. [195] carried out low velocity impact tests on sandwich plates with foam, resin and softwood fillers. This type of sandwich construction was shown to compare favourably to stiffened monolithic steel skins under impact conditions similar to those likely to be encountered on offshore platforms, e.g. a falling drill collar. The most efficient of these fillers in terms of resistance to penetration was found to be softwood. A simple design procedure was proposed which allowed an estimate of the energy absorbing capacity of the panels to be made. A full-scale test in which a drill collar with mass 3560 kg was dropped on to a wood-filled sandwich panel from a height of 15 m (impact energy = 532 kJ) was carried out. The panel had 12 mm thick steel skins, a softwood filler thickness of 240 mm and measured 900 x 900 mm. The sandwich panel absorbed the impact energy without allowing perforation to occur and the final deflection of the bottom skin was similar to that predicted by the theory (98 mm).

7. CONCLUSIONS

7.1. Experimental studies

The quality and quantity of experimental studies on projectile impact on structural elements has been steadily increasing over the last few years. New experimental techniques have been developed and improved instrumentation has allowed more detailed information to be collected. However there are still a number of areas to which little attention has been paid and a number of gaps in the database assembled from those areas of research that have been addressed.

Almost all of the experimental studies have consisted of small scale impact tests, that is, projectiles with diameters up to 15 mm striking targets with thicknesses up to 10 mm and spans up to 500 mm. There has been very little non-military investigation into larger scale impact situations such as those that may be encountered following an explosion of a substantial piece of machinery. The experimental data that have been published concerning projectile impact has been somewhat patchy. The nature of the topic is such that a large number of combinations of projectile and target types are involved and consequently it is rare that any two studies can be directly compared. It is hoped that the section on experimental investigations contains sufficient details concerning the tests that have been carried out to allow any comparison that can be made between them to be identifiable and to highlight the differences in experimental details and methods.

Some observations that were common to a number of investigations can be mentioned. For example, metallic plates when struck by a rigid projectile were seen to experience maximum deflections which increased in magnitude with increasing impact velocity up to the point at which perforation of the plate occurred, whereafter further increase in the impact velocity resulted in a decrease in the maximum plate deflection. Also the velocity drop experienced by the projectile was seen to fall to a minimum value as the impact velocity was increased to just above the target's ballistic limit and then rise monotonically with increasing impact velocity. The different failure modes that occur when a metallic plate is struck by a projectile have been well documented. The type of failure that occurs in metals is primarily dependent on the projectile nose shape, the ratio between the target thickness and the projectile diameter and the material properties of the target material. In general, relatively thin, ductile targets when struck by blunt projectiles fail through discing – a thinning of the plate material under the impact zone leading to tensile tearing. This process is usually accompanied by substantial amounts of global dishing of the target. Thick, brittle targets tend to fail by plugging – a shear-dominated process in which a plug of material is separated from the surrounding target. Sharp-nosed projectiles cause failure by petalling in thin, ductile targets and plugging in thick, brittle targets. In all cases the amount of global deformation experienced by the targets is greatest at the ballistic limit and decreases with increasing impact velocity.

There are a number of factors affecting the penetration and perforation processes that are, at present, not fully understood. For example the role of clamping conditions in determining a target's ballistic limit is unclear. Also the mass of the projectile appears to affect the response of the target to impact, although the manner in which it does has not been determined. Uncertainties over the effect of parameters such as these are the main reasons why direct comparison between different studies can rarely be made.

Recently, some investigations have included information on the details of the failure zone. For example, where plugging has occurred measurements have been made of the plug dimensions and the shear zone width. These results have helped to explain some failure and penetration mechanisms and are also necessary for some analyses which require such data for their solution. However, such information is extremely patchy and shows no clear trend.

The majority of investigations have been concerned with the normal impact of flat plates with rigid projectiles. The number of studies involving oblique impact, projectile yaw or deformable projectiles are far fewer. It has been shown that obliquity does not significantly affect the ballistic limit of a metal plate provided the angle of obliquity is less than 30o. Greater angles than this increase the target's ballistic limit, unless the presence of projectile yaw causes a change in the failure mode of the target, in which case the increase in angle of obliquity may lower its ballistic limit. The occurrence of projectile deformation raises the ballistic limit of a target.

Other areas of interest have included the impact of multi-layered plates and the impact of tubes. The benefits of using multi-layered plates as opposed to monolithic plates are unclear, with the limited number of investigations reaching no firm conclusions. The investigations into the response of steel tubes to projectile impact indicate that they experience failure modes similar to those experienced by flat steel plates, with these failure modes also being dependent on the relative tube wall thickness, projectile nose shape and tube material. A similar dependence of ballistic limit on projectile mass was shown. The global response of the tube was, unlike the plates, non-axisymmetric, with the tube wall behaving in a stiffener manner than an equal thickness steel plate.

Although all the experimental studies have involved almost exclusively, small scale impact tests there has been a dearth of investigation into the applicability of scaling laws to allow the results of these studies to be applied to large scale situations. The possible presence of factors such as strain-rate effects and ductile – brittle transition zones suggests that scaling must be carried out with extreme caution and, until hard experimental evidence is provided to prove otherwise, this will continue to be the case.

7.2. Prediction of ballistic limit

The ability to predict a target's ballistic limit under a certain set of impact conditions has been the goal of impact engineers since the problems arising from projectile perforation were first identified. The use of empirical equations were the engineer's first tool, and they remain a very important one. Various studies have shown that, provided the impact conditions lie within the parameters stated for the formula to be used, an empirical formula is a quick and effective means of predicting a target's ballistic limit. A major drawback with them is that the small number of formulae available from non-military sources only cover a limited range of impact conditions.

There has been considerable attention paid to the development of analytical models over the past few years. When a projectile strikes a target with a velocity considerably greater than the target's ballistic limit the older analyses, such as those by Recht and Ipson [32], Thompson [90] and Zaid and Paul [94], which ignore global effects and assume a constant projectile velocity throughout the penetration process, are fairly accurate in predicting the velocity drop experienced by the projectile. If the ballistic limit of the target plate is known, the analysis of Recht and Ipson [32] successfully predicts the velocity drop at all impact velocities.

Analytical models that predict the ballistic limit of a structure are continually being developed in order to represent more accurately the phenomena associated with projectile impact. A number of models that are simple to apply but fairly crude in their representation of the penetration process are available. For example the models of Thompson [90] or Woodward [91] may be used to obtain a first approximation of the energy required to perforate a thin plate by ductile hole enlargement. Similarly an estimation of the energy required for failure by plugging can be obtained using Woodward's analysis [100]. These models, which are for conically-tipped projectiles, are quick and easy to use but are fairly conservative, tending to under-predict the ballistic limit by neglecting various energy absorbing mechanisms (e.g. global target response).

The use of multi-stage penetration models to analyse projectile penetration into a target was first attempted by Awerbuch [128]. Since then they have been improved by better representation of the various local phenomena, and also by the inclusion of global effects. Where global effects are likely to be dominant, the analyses of Shadbolt et al. [131] or Woodward [134], which model the global response of plate coupled with a fairly simple failure criterion at the point of loading, may be used to estimate the energy absorbing properties of the target. These latter models are more sophisticated in their representation of projectile impact than the relatively simple models of Thompson [90] and Woodward [91,100], but have the disadvantage of requiring computer facilities for their solution and, in most cases, some experimentally obtained data.

Recently plastic wave theory has been successfully applied to the problem of projectile penetration. This approach is suitable for relatively thick plates (relative to projectile diameter) when struck by flat faced projectiles. When account is taken of global deformation of the plate (bending or shear) this approach is seen to improve upon the simpler models in predicting the response of the plate, especially when the projectile impact velocity is very close to the ballistic limit of the target. Plastic wave theory is the most successful analytical method for predicting the profiles adopted by the plate during impact.

In order for any of the above models to be successfully applied to a given situation a certain amount of qualitative judgement is required by the user. Each analysis is only applicable for a given range of impact conditions and most presuppose the mode of failure. It is therefore necessary to select the most apt analysis depending on the predicted mode of failure, the type of projectile likely to be encountered (mass, diameter, nose-shape, deformability, angle of flight, etc.) and the type of target response likely to occur (localized, global, or a combination of the two). Choosing an unsuitable model may lead to gross errors in predicting a target's ballistic limit.

Another problem that is encountered when applying the various analyses to a given problem is the choice of material properties. The presence of factors such as strain-rate effects, strain-hardening, friction and lateral constraint indicate that a target's material properties may alter significantly during the penetration process, and if account is not taken of these effects then substantial errors may accrue. In addition, account will need to be taken of any anisotropy in the material properties.

7.3. Prediction of target response and impact loads

Various methods that predict the plate profile and maximum deflection of a target when struck by a non-perforating projectile have been described. Investigations into the impulsive loading of plates have shown that the response of thin plates to this type of loading is dominated by membrane effects. Analyses that are based on a bending-dominated mode of failure, such as that by Calder et al. [114] have been shown to be applicable only for small deflections. Beynet and Plunkett [11] provide an analysis, based on a membrane-dominated model, which accurately predicts the response of thin plates to projectile impact. A simpler method that may be used to predict the plate deflection (for thin plates) is that of Calder and Goldsmith [15] which assumes the form of the deformed plate profile but gives reasonable estimates of maximum deflection.

An estimate of the forces generated during the impact process can be readily obtained using the method described by Levy and Goldsmith [127]. Although their method, which reduces the projectile - target system to a number of lumped-parameters, is based on a very elementary one-dimensional analysis of the penetration and perforation processes involved, it is seen to give accurate predictions of the force and central plate deflection histories. It has the advantage of being much simpler to implement than other more detailed approaches and it is completely predictive for sub-ballistic limit impacts. Perforating impact situations require measured information from the perforated specimen.

7.4. Prediction of pipe response to impact

There has been very little attempt at analysing the response of tubes to projectile impact. Empirical relationships have been proposed by Stronge [85] and Neilson et al. [61] and these are suitable for predicting the minimum energy required for perforation of steel tubes when the impact conditions lie within the stated ranges. Analytical models that successfully predict target response have not yet been developed although the string-on-foundation analogy may be used to predict central deflections of the pipe wall under projectile impact [121,124]. Alternatively a quasi-static analysis (for example [53]) may be used to predict low velocity impact behaviour. Numerical solutions have been shown to predict target response reasonably accurately [152], although prediction of failure of the tube wall has not yet been achieved.

7.5. Response of concrete and steel – concrete composite structures to impact

Concrete is a material that is suitable for use for impact protection where weight and space are not limited. The ballistic limit and failure mechanisms of concrete structures are dependent on the amount and type of reinforcement. Concrete tends to be less sensitive to impact conditions (such as projectile nose-shape, impact velocity, projectile mass) than monolithic steel structures and hence can be used with greater confidence when the impact conditions are not known in advance. It has been shown that concrete can be used to clad steel structures in order to protect the steel from adverse impact conditions such as sharp-nosed, high velocity projectiles.

Predictions of the ballistic limit of concrete structures are predominantly empirical, with the NDRC formula [184] generally being regarded as the most acceptable.

REFERENCES

[1]	W.Johnson. Impact Strength of Materials. Edward Arnold (1972).

[2]	M.E.Backman and W.Goldsmith. The mechanics of penetration of projectiles into targets. Int. J. F.ngng Sci. 16, 1 – 99 (1978).

[3]	W.Johnson, N.R.Chitkara, A.H.Ibrahim and A.K.Dasgupta. Hole flanging and punching of circular plates with conically headed cylindrical punches. inst. Mech. Engrs J. Strain Analysis 8, 223 241 (1973).

[4]	W.Johnson, S.K.Ghosh and S.R.Reid. Piercing and hole-flanging of sheet metals: a survey. Memoires Scientifiques Revue Metallurgic, pp. 585 – 606, April (1980).

[5]	S.K.Ghosh and W.Johnson. Quasi-static and dynamic perforation of thin aluminium plates. Aluminium 56, 142 -146 (1980).

[6]	C.W.Young. Depth prediction for earth penetrating projectiles. Proc. ASCE 95 SM3, 803--817 (1969).

[7]	W.Johnson. Some conspicuous aspects of the century of rapid changes in battleship armours, ca 1845 – 1945. Int. J. impact Engng 7, 261 – 284 (1988).

[8]	W.Goldsmith and S.A.Finnegan. Penetration and perforation processes in metal targets at and above ballistic limits. Int. i. Mech. Sci. 13, 843 – 866 (l971).

[9]	R.S.J.Corran, P.J.Shadbolt and C.Ruiz. Impact loading of plates – an experimental investigation. lnt J. Impact Engng 1, 3-22 (1983).

[10]	A.I.O.Zaid and F.W.Travis. Conf. on the Mechanical Properties of Materials at High Rates of' Strain, Conference series No. 21, pp. 417 – 428 (Edited by J. Harding). Institute of Physics, London (1974).

[11]	P.Beynet and R.Plunkett. Plate impact and plastic deformation by projectiles. F.xp. Mech. 11, 64 – 70 (1971).

[12]	N.R.Chitkara and W.Johnson. Hole flanging and piercing of circular plates. Sheet Metal Ind., pp. 635 – 640, October (1974).

[13]	W.Johnson, N.R.Chitkara and P.A.Bex. Characteristic features in the hole flanging and piercing of thin and thick circular plates using conical and ogival punches. Paper 142 Proc. 15 th Int. M TDR Conf., pp. 695 – 701, (Edited by S. A. Tobias and F. Koenigsberger). Macmillan (1974).

[14]	W.Johnson and A.G.Mamalis. The perforation of circular plates with four-sided pyramidally-headed square-section punches. Int. J. Mech. Sci. 20, 849-866 (1978).

[15]	C.A.Calder and W.Goldsmith. Plastic deformation and perforation of thin plates resulting from projectile impact. Int. J. Solids Struct. 7, 863 - 881 (1971).

[16]	N.Levy and W.Goldsmith. Normal impact and perforation of thin plates by hemispherically tipped projectiles. Int. J. Impuct Engng 2, 299 – 324 (1984).

[17]	I.G.Crouch, B.J.Baxter and R.L.Woodward. Empirical tests of a model for thin plate perforation. Int. J. Impact Engng 9, 19-33 (1990).

[18]	S.Leppin and R.L.Woodward. Perforation mechanisms in thin titanium alloy targets. 1nt. J. Impact Ending 4, 107 – 115 (1986).

[19]	W.Goldsmith. In Metal Forming and Impact Mechanics, pp. 271 – 287 (Edited by S. R. Reid). Pergamon Press (1985).

[20]	C.Palomby and W.J.Stronge. Blunt missile perforation of thin plates and shells by discing. Int. J, impact Engng 7, 85 – 100 (1988).

[21]	L.Sangoy, Y.Meunier and G.Pont. Steels for ballistic protection. Israel J. Technolvgy 24, 319 – 326 (1988).

[22]	M.Langseth and P.K.Larsen. Dropped objects plugging capacity of steel plates: an experimental investigation. Int. J. Impuct Engng 9, 289 – 316 (1990).

[23]	M.Langseth and P.K.Larsen. The behaviour of square steel plates subjected to a circular blunt ended load. Int J. impact Engng 12, 617 – 638 (1992).

[24]	P.C.Chou, J.Hashemi, A.Chou and H.C.Rogers. Experimentation and finite element simulation of adiabatic shear bands in controlled penetration impact. Int. J. Impact F.ngng 11, 305 – 321 (1991).

[25]	V.V.Astanin, Sh.U.Galiev and K.B.Ivashchenko. Cone formation in targets beneath a penetrating projectile. Int. J. Impuct Engng 11, 515- 525 (1991).

[26]	I.Marom and S.R.Bodner. Projectile perforation of muli-layered beams. Int. J. Mech. Sci. 21, 489 – 504 (1979).

[27]	R.L.Woodward, S.R.Tracey and I.G.Crouch. The response of homogeneous and laminated metallic sheet material to ballistic impact. J. de Physique Vl Colloque C3 1, C3 277 -C3 282 (1991).

[28]	J.Radin and W.Goldsmith. Normal projectile penetration and perforation of layered targets. Int. J. Impact Engng 7, 229 – 259 (1988).

[29]	J.G.Hetherington and B.P.Rajagopalan. An investigation into the energy absorbed during ballistic perforation of composite armours. Inr. J. Impact Engng 11, 33 – 40 (1991).

[30]	A.L.Florence. Interaction of projectiles and composite armour, part II. Stanford Research Institute, Menlo Park, AMMRC-CR-69-15, August (1969).

[31]	C.Navarro, M.A.Martinez, R.Cortes and V.Sanchez-Galvez. Some observations on the normal impact on ceramic-faced armours backed by composite plates. Int. J. impact Engng 13, 145 – 156 (1993).

[32]	R.F.Recht and T.W.Ipson. Ballistic perforation dynamics. J. Appl. Mech. 30, 385 – 391 (1963).

[33]	M.Zaid and B.Paul. Oblique perforation of a thin plate by a truncated conical projectile. J. Franklin Inst. 268, 24 – 45 (1959).

[34]	J.Awerbuch and S.R.Bodner. An investigation of oblique perforation of metallic plates by projectiles. Exp. Mech. 17, l47 – I S3 (l 977).

[35]	N.K.Gupta and V.Madhu. Normal and oblique impact of a kinetic energy projectile on mild steel plates. Int. J. impact Engng 12, 333 – 344 (1992).

[36]	R.L.Woodward and N.J.Baldwin. Oblique perforation of targets by small armour piercing projectiles. J. Mech. Engng Sci. 21, 85 – 91 (1979).

[37]	W.Goldsmith and S.A.Finnegan. Normal and oblique impact of cylindro-conical and cylindrical projectiles on metallic plates. Int. J. Impact Engny 4, 83 – 105 (1986).

[38]	S.P.Virostek, J.Dual and W.Goldsmith. Direct force measurements in normal and oblique impact of plates by projectiles. Int. J. impact Engng 6, 247 – 269 (1987).

[39]	S.P.Virostek. Ms Thesis, University of California, Berkeley (1986).

[40]	J.A.Zukas. In Impact Dynamics, pp. 155 – 214 (Edited by J. A. Zukas et al.). John Wiley (1982).

[41]	C.Grabarek. Joint Technical Coordinating Group for Munitions Effectiveness (J TCG/ME), Ballistic Research Laboratories, Aberdeen Proving Ground, MD, U.S.A. (1973).

[42]	S.J.Bless, J.P.Barber, R.S.Bertke and F.W.Swift. Penetration mechanics in yawed rods. Int. J. Engng Sci. 16, 829 – 834 (1978).

[43]	E.Wu and W.Goldsmith. Normal impact of blunt projectiles on moving targets. Experimental study. Int. J. Impact Engng 9, 389 – 404 (1990).

[44]	E.Wu and W.Goldsmith. Normal impact of blunt projectiles on moving targets. Analytical considerations. lnt. J. Impact Engng 9, 405 - 432 (1990).

[45]	S.T.S.Al-Hassani, S.A.L.Salem and W.Johnson. The cratering of stationary and slowly moving targets by a high speed water jet. J. Ballistics 4, 909 – 933 (1980).

[46]	W.Johnson, S.R.Reid and S.K.Ghosh. Piercing of cylindrical tubes. Century 2 Pressure Vessel & Piping Conf., ASME., San Fransisco, CA, U.S.A. August 12 – 15 (1980); also J. Press. Vess. Tech., ASME 103,255 – 260 (1981).

[47]	W.Johnson, S.K.Ghosh, A.G.Mamalis, T.Y.Reddy and S.R.Reid. The quasi-static piercing of cylindrical tubes or shells. Int. J. Mech. Sci. 22, 9 – 20 (1980).

[48]	S.K.Ghosh, W.Johnson, S.R.Reid and T.X.Yu. On thin rings and short tubes subjected to centrally opposed concentrated loads. Int. J. Mech. Sci. 23, 183 – 194 (1981).

[49]	S.G.Thomas, S.R.Reid and W.Johnson. Large deformations of thin-walled circular tubes under transverse loading. Part I. Int. J. Mech. Sci. 18, 325 – 333 (1976).

[50]	A.R.Watson, S.R.Reid and W.Johnson. Large deformations of thin-walled circular tubes under transverse loading. Part II. Int. J. Mech. Sci. 18, 387 – 397 (1976).

[51]	A.R.Watson, S.R.Reid, W.Johnson and S.G.Thomas. Large deformations of thin-walled circular tubes under transverse loading. Part III. Int. J. Mech. Sci. 18, 501 – 509 (1976).

[52]	J. de Oliveira, T.Wierzbicki and W.Abramowicz. Plastic behaviour of tubular members under lateral concentrated loading. Nor. Veritas Tech. Rep. 82 – 0708 (1982).

[53]	N.Jones and W.Q.Shen. A theoretical study of the lateral impact of fully clamped pipelines. Proc. Inst. Mech. Engrs 206 (E), 129 – 146 (1992).

[54]	S.R.Reid and K.Goudie. Denting and bending of tubular beams under local loads. In Structural Failure, pp. 331 – 364 (Edited by T. Wierzbicki, and N. Jones). John Wiley (1989).

[55]	C.G.Soares, and T.H.Qreide. Plastic analysis of laterally loaded circular tubes. J. Structural Engng, ASCE 109, 451 – 467 (1983).

[56]	C.P.Ellinas. Ultimate strength of damaged tubular bracing members.. .JStructural Engng, ASCE 110,245 – 259 (1983).

[57]	D.M.Richards and A.Andricou. Residual strength of dented tubulars: impact energy correlation. J. Energy Resources Tech. 107, 485 – 492 (1985).

[58]	J.Taby and T.Moan. Collapse and residual strength of damaged tubular members. BOSS'85, Paper B8 (1985).

[59]	S.Durkin. An analytical method for predicting the ultimate capacity of a dented tubular member. Int. J. Mech. Sci. 29, 449 – 467 (1987).

[60]	Ma Xiaoqing and W.J.Stronge. Spherical missile impact and perforation of filled steel tubes. Int. J. Impact Engng 3, 1 – 16 (1985).

[61]	A.J.Neilson, W.D.Howe and G.P.Garton. Impact resistance of mild steel pipes: an experimental investigation. UKAEA Report AEEW-R 2125 (1987).

[62]	G.G.Corbett, S.R.Reid and S.T.S.Al-Hassani. Static and dynamic penetration of steel tubes by hemispherically nosed punches. Int. J. Impact Engng 9, 165 – 190 (1990).

[63]	M.J.Manjoine. Influence of rate of strain and temperature on yield stresses of mild steel. J. Appl. Mech. 66, A211 – A218 (1944).

[64]	W.Johnson. Private communication.

[65]	T.Nicholas. In Impact Dynamics, pp. 277 – 332 (Edited by J. A. Zukas et al.). John Wiley (1982).

[66]	S.T.S.AL-Hassani and S.R.Reid. The effects of high strain rate on material properties. Joint Industry Project on Blast and Fire Engineering for Topside Structures. Steel Construction Institute Report (Blast Response Series) BR4 (1992).

[67]	T.Nicholas and A.M.Rajendran. In High Velocity Impact Dynamics, pp. 127 – 296 (Edited by J. A. Zukas). John Wiley (1990).

[68]	R.L.Woodward. Penetration of semi-infinite metal targets by deforming projectiles. Int. J. Mech. Sci. 24, 73 – 87(1982).

[69]	R.L.Woodward and M.E. de Morton. Penetration of targets by flat-ended projectiles. Int. J. Mech. Sci. 18, 119 – 127 (1976).

[70]	J.Liss, W.Goldsmith and F.E.Hauser. Constraint to side flow in plates. J. Appl. Mech. 50, 694 – 698 (1983).

[71]	J.M.Krafft. Surface friction in ballistic penetration. J. Appl. Phys. 26(10), 1248 – 1253 (1955).

[72]	B.Robins. New Principles of Gunnery, London (1742).

[73]	D.G.Christopherson. Structural Defence, 1945. Ministry of Home Security, Research and Experiments Department, (R. C. 450) January (1946).

[74]	W.E.Baker, P.S.Weshire and P.T.Dodge. Similarity Methods in Engineering Dynamics: Theory and Practice of Scale Modelling. Spartan Books, Rocheele Park, N 1 (1973).

[75]	N.Jones. In Structural Impact and Crashworthiness, Vol. 1, pp. 45 – 74 (Edited by G. A. O. Davies). Elsevier Applied Science (1984).

[76]	P.R.B.Dallard and J.C.Miles. In Structural Impact and Crashworthiness, Vol. 2, pp. 369 – 382. (Edited by J. Morton). Elsevier Applied Science (1984).

[77]	E.Booth, D.Collier and J.C.Miles. In Structural Crushworthiness, pp. 136-174 (Edited by N. Jones and T. Wierzbicki). Butterworth (1983).

[78]	T.A.Duffey, M.C.Cheresh and S.H.Sutherland. Experimental verification of scaling laws for punch-impact-loaded structures. Int. J. Impact Engng 2, 103 – 117 (1984).

[79]	C.E.Anderson Jr.S.A.Mullin and C.J.Kuhlman. Computer simulation of strain rate effects in replica scale model penetration experiments. Int. J. Impact Engng 13, 35 – 52 (1993).

[80]	S.Ohte, H.Yoshizawa, N.Chiba and S.Shida. Impact strength of steel plates struck by projectiles. Bull. JSME 25.206 1226-1231 (1982).

[81]	A.J.Neilson. Empirical equations for the perforation of mild steel plates. Int. J. Impact Engng 3, 137 – 142 (1985).

[82]	J.Jowett. The effects of missile impact on thin metal structures. UKAEA Safety and Reliability Directorate Report No. S. R. D. R 378 (1986).

[83]	H-M.Wen and N.Jones. Semi-empirical equations for the perforation of plates struck by a mass. In Structures Under Shock and Impact Il, pp. 369 – 380 (Edited by P. S. Bulson). Computational Mechanics Publications (1992).

[84]	G.G.Corbett and S.R.Reid. Quasi-static and dynamic local loading of monolithic simply-supported steel plates. Int. J. 1mpact Engng 13, 423 – 441 (1993).

[85]	W.J.Stronge. In Metal Forming and Impact Mechanics, pp 389 – 402 (Edited by S. R. Reid). Pergamon Press (1985).

[86]	A.I.O.Zaid, A.El-Kalay and F.W.Travis. An examination of the perforation of a mild steel plate by a flat-ended cylindrical projectile. Int. J. Mech. Sci. 15, 129 – 143 (1973).

[87]	G.I.Taylor, The formation and enlargement of a circular hole in a thin plastic sheet. Quart J. Mech. Appl. Math. 1, 103 – 124 (1948).

[88]	W.Frieberger. A problem in dynamic plasticity: the enlargement of a circular hole in a flat sheet. Prvc. Camb. Phil. Soc. 48, 135 – 148 (1952).

[89]	S.Kumari. The finite expansion of a circular hole in an infinite plate: a dynamic solution. Int. J. Mech. Sci. 17, 23 – 29 (1975).

[90]	W.T.Thompson. An approximate theory of armour penetration. J. Appl. Phys. 26 (1), 80 – 82 (1955).

[91]	R.L.Woodward. The penetration of metal targets by conical projectiles. lnt. J. Mech. Sci. 20, 349 – 359 (1978).

[92]	R.Hill. A theory of the plastic bulging of a metal diaphragm by lateral pressure. Phil. Mag. 40, 971-983 (1949).

[93]	M.S.Sodha and V.K.Jain. On physics of armour penetration. J. Appl. Phys. 29, 1769 – 1770 (1958).

[94]	M.Zaid and B.Paul. Mechanics of high speed projectile perforation. J. Franklin Inst. 264, 117 – 126 (1957).

[95]	B.Paul and M.Zaid. Normal perforation of a thin plate by truncated conical projectiles. J. Franklin Inst. 265, 317-336(1958).

[96]	W.Goldsmith, T.W.Liu and S.Chulay. Plate impact and perforation by projectiles. Exp. Mech. 5, 385 – 404 (1965).

[97]	R.F.Recht. Catastrophic thermoplastic shear. J. Appl. Mech. 31, 189 – 193 (1964).

[98]	T.A.C.Stock and K.R.L.Thompson. Penetration of aluminium alloys by projectiles. Metallurgical Trans 1, 219 – 224 (1970).

[99]	J.W.Lethaby and I.C.Skidmore. The deformation and plugging of thin plates by projectile impact. Conf. on Mech. Prop. of Materials at High Rates of Strain, pp. 429 – 441, Oxford, April (1974).

[100]	R.L.Woodward. The penetration of metal targets which fail by adiabatic shear plugging. Int. J. Mech. Sci. 20 599 – 607(1978).

[101]	R.L.Woodward. The interrelation of failure modes observed in the penetration of metallic targets. Int. J. Impact Engng 2, 121 – 129 (1984).

[102]	Y.L.Bai and W.Johnson. Plugging: physical understanding and energy absorption. Metals Tech. 9, 182 – 190 (1982).

[103]	T.M.Chang and H.W.Swift. Shearing of metal bars. J. Inst. Metals 78, 119 – 146 (1950).

[104]	W.Johnson and R.A.C.Slater. A survey of the slow and fast blanking of metals at ambient and high temperatures. In Proc. Int. Conf. Manufacturing Tech, pp. 825 – 851, CIRP-ASTME (1967).

[105]	B.Landkof and W.Goldsmith. Petalling of thin, metallic plates during penetration by cylindro-conical projectiles. Int. J. Solids Struct. 21, 245 266 (1983).

[106]	E.W.Parkes. The permanent deflection of a cantilever struck transversely at its tip. Proc. Roy. Soc. A228, 462 – 476 (1955).

[107]	A.L.Florence. Circular plate under uniformly distributed impulse. Int. J. Solids Struck. 2, 37 – 47 (1966).

[108]	N.Jones. Finite deflections of a rigid-viscoplastic strain hardening annular plate loaded impulsively. J. Appl. Mech. 35, 349 – 356 (1968).

[109]	J.K.Dienes and J.W.Miles. A membrane model for the response of thin plates to ballistic impact. J. Mech. Phys. Solids 25, 237 – 256 (1977).

[110]	G.N.Nurick and J.B.Martin. Deformation of thin plates subjected to impulsive loading – a review. Part I: theoretical considerations. Int. J. Impact Engng 8, 159 – 170 (1989).

[111]	G.N.Nurick and J.B.Martin. Deformation of thin plates subjected to impulsive loading – a review. Part II: experimental studies. Int. J. Impact Engng 8, 171 186 (1989).

[112]	T.Wierzbicki and J.M.Kelly. Finite deflections of a circular viscoplastic plate subject to projectile impact. lnt. J. Solids Struct. 4, 108 l -1092 (1968).

[113]	E.T.Onat and R.M.Haythornthwaite. The load carrying capacity of circular plates at large deflections. J. Appl. Mech. 23, 49 55 (1956).

[114]	C.A.Calder, J.M.Kelly and W.Goldsmith. Projectile impact on an infinite viscoplastic plate. Int. J. Solids Struct. 7, 1143 1 152 (1971).

[115]	J.M.Kelly and T.R.Wilshaw. A theoretical and experimental study of projectile impact on clamped circular plates. Proc. Roy. Soc. A 306, 435 – 447 (1968).

[116]	C.P.Ellinas and A.C.Walker. Damage on offshore tubular bracing members. Proc. IABSE Colloquium on Ship Collision with Bridges and Offshore Structures, pp. 253 – 261, Copenhagen (1983).

[117]	T.Wierzbicki and M.S.Suh. Indentation of tubes under combined loading. Int. J. Mech. Sci. 30, 229 – 248 (1988).

[118]	Y.Bai and P.T.Pederson. Elastic plastic behaviour of onshore steel structures under impact loads. Int. J. Impact Engng 13, 99-115 (1993).

[119]	C.R.Calladine. Thin-walled elastic shells analysed by a Rayleigh method. Int. J. Solids Struct. 13, 515 -530 (1977).

[120]	S.R.Reid. Influence of geometrical parameters on the mode of collapse of a "pinched" rigid-plastic cylindrical shell. Int. J. Solids Struct. 14, 1027 – 1043 (1978).

[121]	T.X.Yu and W.J.Stronge. Large deflections of a rigid plastic beam-on-foundation from impact. Int. J. Impact Engng 9, 115 – 126 (1990).

[122]	W.J.Stronge. Impact on metal tubes: indentation and perforation. In Structural Crashworthiness and Failure, pp. 165 – 188 (Edited by N. Jones and T. Wierzbicki). Elsevier Applied Science (1993).

[123]	T.Wierzbicki and M.S.Hoo Fatt. Impact response of a string-on-foundation. Int. J. Impact Engng 12, 21 – 36 (1992).

[124]	T.Wierzbicki and M.S.Hoo Fatt. Damage assessment of cylinders due to impact and explosive loading. Int. J. Impact Engng 13, 215 – 242 (1993).

[125]	H.Stolarski. Assessment of large displacements of a rigid – plastic shell withholding a localised impact. Nuc. Engng und Design 41, 327 – 334 (1977).

[126]	J.V.Poncelet. Rapport sur un memoire de MM. Piobert et Morin. Mem. Acad. Sci. 15, 55 – 91 (1835).

[127]	N.Levy and W.Goldsmith. Normal impact and perforation of thin plates by hemispherically tipped projectiles. Int. J. Impact Engng 2, 209 – 229 (1984).

[128]	J.Awerbuch. A mechanics approach to projectile penetration. Israel J. Tech. 8, 375 – 383 (1970).

[129]	J.Awerbuch, S.R.Bodner. Analysis of the mechanics of perforation of projectiles in metallic plates. Int. J. Solids Struct. l0 (1), 671 – 684 (1974).

[130]	J.Awerbuch and S.R.Bodner. Experimental investigation of normal perforation of projectiles into metallic plates. Int. J. Solids Struct. 10 (1), 685 699 (1974).

[131]	P.J.Shadbolt, R.S.J.Corran and C.Ruiz. A comparison of plate perforation models in the sub-ordnance range. Int. J. Impact Engng 1, 23 -49 (1983).

[132]	R.S.J.Corran. Comment. Int. J. Impact Engng 2, 283 (1984).

[133]	E.Reissner. On finite deflections of circular plates. Amer. Math. Soc., Proc. Symp. Appl. Math. 1, 213 – 219 (1949).

[134]	R.L.Woodward. A structural model for thin plate perforation by normal impact of blunt projectiles. Int. J. Impact Engng 6, 129 – 140 (1987).

[135]	P.S.Symonds. Engineering Plasticity, pp. 647 664 (Edited by Heyman and Leckie). Cambridge University Press (1968).

[136]	J.Quanlin. Dynamic response of an infinitely large rigid plastic plate impacted by a rigid cylinder with transverse shear and rotatory inertia. Int. J. Impact Engng 7, 391 – 400 (1988).

[137]	J.Liss, W.Goldsmith and J.M.Kelly. A phenomenological penetration model of plates. Int. J. Impact Engng 1 (4), 321 – 341 (1983).

[138]	J.F.Heyda et. al. A combined theoretical and experimental investigation of armor penetration mechanics. AFATL-TR-70-78, Air force Armament Lab Eglin Air Force Base, Florida (1970).

[139]	J.Liss and W.Goldsmith. Plate perforation phenomena due to normal impact of blunt cylinders. Int. J. Impact Engng 2, 37 – 64 (1984).

[140]	Yuan Wenxue, Zhou Lanting, Ma Xiaoqing and W.J.Stronge. Plate perforation by deformable projectiles – a plastic wave theory. Int. J. Impact Engng 1, 393 – 412 (1983).

[141]	S.T.Jenq, W.Goldsmith and J.M.Kelly. Effect of target bending in normal impact of a flat-ended cylindrical projectile near the ballistic limit. Int. J. Solids Struct. 24, 1243 – 1266 (1988).

[142]	M.Shoukry, S.Nair and S.Kalpakjian. Effect of shear deformation on the dynamic plastic bending of metallic plates during normal penetration. Int. J. Engng Sci. 29, 1035 – 1052 (1991).

[143]	G.H.Jonas and J.A.Zukas. Mechanics of penetration: analysis and experiment. Int. J. Engng Sci. 16, 879 – 904 (1978).

[144]	M.L.Wilkins. Mechanics of penetration and perforation. Int. J. Engng Sci. 16, 793 – 807 (1978).

[145]	J.A.Zukas. In Impact Dynamics, pp. 367 – 447 (Edited by J. A. Zukas et. al.). John Wiley (1982).

[146]	J.A.Zukas. In High Velocity Impact Dynamics, pp. 593 – 714 (Edited by J. A. Zukas). John Wiley (1990).

[147]	A.De Rouvray, F.Arnaudeau, J.Dubois, J.F.Chedmail and E.Haug. In Structural Impact and Crashworthiness, Vol. 1, pp. 193 – 242 (Edited by G. A. O. Davies). Elsevier Applied Science (1984).

[148]	L.E.Schever, N.J.Salamon and W.K.Liu. Computational Techniques for Contact, Impact, Penetration and Perforation of Solids. ASME. (1988).

[149]	C.E.Anderson and S.R.Bodner. Ballistic impact: the status of analytical and numerical modelling. Int. J. Impact Engng 7, 9 – 36 (1988).

[150]	A.J.Neilson. Missile impact on metal structures. Nuclear Energy 19 (3), 191 – 198 (1980).

[151]	S.P.Timoshenko and S.Woinowsky-Krieger. Theory of Plates and Shells. McGraw Hill (1970).

[152]	A.J.Neilson. Hard missile impact on plates and tubes. Seminar on The State-of-the-Art in the Simulation of Impulsive and Impact Loadings, St Peter's College, Oxford, July (1983).

[153]	L.E.Schwer, B.S.Holmes and S.W.Kirkpatrick. Response and failure of metal tanks from impulsive spot loading: experiments and calculations. 1nt. J. Solids Struct. 24 (8), 817 – 833 (1988).

[154]	D.J.Bamman, M.L.Chiesa, M.F.Horsemeyer and L.I.Weingarten. Failure in ductile materials using finite element methods. In Structural Crashworthiness and Failure, pp. 1 – 54, (Edited by N. Jones and T. Wierzbicki). Elsevier Applied Science (1993).

[155]	M.J.Forrestal, D.B.Longcope and F.R.Norwood. A model to estimate forces on conical penetrators into dry, porous rock. J. Appl. Mech. 48, 25 – 29 (1981).

[156]	D.B.Longcope and M.J.Forrestal. Closed-form approximations for forces on conical penetrators into dry, porous rock. J. AppL Mech. 48, 971 – 972 (1981).

[157]	M.J.Forrestal, F.R.Norwood and D.B.Longcope. Penetration into targets described by locked hydrostats and shear strength. Int. J. Solids Stuct. 17, 915 – 924 (1981).

[158]	D.B.Longcope and M.J.Forrestal. Penetration of targets described by a Mohr – Coulomb failure criterion with a tension cutoff. J. Appl. Mech. 50, 327 – 333 (1983).

[159]	M.J.Forrestal. Penetration into dry porous rock, Int. J. Solids Struct. 22, 1485 – 1500 (1986).

[160]	C.E.Anderson and J.D.Walker. An examination of long-rod penetration. Int. J. 1mpact Engng 11, 481 – 501 (1991).

[161]	M.J.Forrestal and V.K.Luk. Penetration into soil targets. Int. J. Impact Engng 12, 427 – 444 (1992).

[162]	J.D.Cinnamon, S.E.Jones, J.W.House and L.L.Wilson. A one-dimensional analysis of rod penetration. Int. J. Impact Engng 12, 145 – 166 (1992).

[163]	V.Hohler and A.J.Stilp. In High Velocity Impact Dynamics, pp. 321 – 404 (Edited by J. A. Zukas). John Wiley(1990).

[164]	M.J.Forrestal, L.M.Lee, B.D.Jenette and R.E.Setchell. Gas-gun experiments determine forces on penetrators into geological targets. J. Appl. Mech. 51, 602 – 607 (1984).

[165]	M.J.Forrestal, L.M.Lee and B.D.Jenrette. Laboratory scale experiments into geological targets to impact velocities of 2.1 km/s. J. Appl. Mech. 53, 317 – 320 (1986).

[166]	L.Thigpen. Projectile penetration of elastic – plastic earth media. Proc. ASCE 100, GT3, 279 – 294 (1974).

[167]	R.T.Sedgewick, L.J.Hageman, R.G.Herrman and J.L.Waddel. Numerical investigations in penetration mechanics. Int. J. Engng Sci. 16, 859 – 869 (1978).

[168]	W.Johnson. Historical and present-day references concerning impact on wood. Int. J. Impact Engng 4, 161 – 184(1986).

[169]	S.R.Reid, C.Peng and T.Y.Reddy. Dynamic uniaxial crushing and penetration of wood. Mechanical Properties of Materials at High Rates of Strain, pp. 535 – 542. Inst of Physics, Conference Series No. 102 (Edited by J. Harding). Institute of Physics, Bristol (1989).

[170]	Z.Rosenberg and Y.Yeshutun. The relation between ballistic efficiency and compressive strength of ceramic tiles. Int. J. Impact Engng 7, 357 – 362 (1988).

[171]	Z.Rosenberg and T.Tsalial. Applying Tate's model for the interaction of long rod projectiles with ceramic targets. Int. J. Impact Engng 9, 247 – 251 (1990).

[172]	R.L.Woodward. A simple one-dimensional approach to modelling ceramic composite armour defeat. Int. J. Impact Engng 9, 455 – 474 (1990).

[173]	C.E.Anderson and B.L.Morris. The ballistic performance of confined Al2O3 ceramic tiles. Int. J. Impact Engng 12, 167 – 187 (1992).

[174]	P.W.Manders, M.G.Bader, M.J.Hinton and D.Q.Flower. Mechanisms of impact damage in filament-wound glass-fibre/epoxy resin tubes. Proc. 3rd Int. Conf on Mechanical Behaviour of Materials (ICH3), pp. 275 – 284, Cambridge (1979).

[175]	G.Dorey. In Structural Impact and Crashworthiness, Vol. 1, pp. 155 – 192 (Edited by G. A. 0 Davies). Elsevier Applied Science (1984).

[176]	G. Clarke. Modelling of impact damage in composite laminates. Composites 20 (3), 209 – 214 (1989).

[177]	K.Ainsworth and K.E.Evans. The measurement and modelling of filament wound pipes undergoing transverse impact. Proc. Inst. Mech. Engrs Paper C400/048, 143 – 148 (1990).

[178]	G.G.Corbett and S.R.Reid. Failure of composite pipes under local loading with a hemispherically-tipped indenter. Int. J. Impact Engng 15, 465 – 490 (1994).

[179]	P.Robinson and G.A.O.Davies. Impactor mass and specimen geometry effects in low velocity impact of laminated composites. Int. J. Impact Engng 12, 189 – 207 (1992).

[180]	W.Goldsmith and J.L.Sackman. An experimental study of energy absorption in impact on sandwich plates. Int. J. Impact Engng 12, 241 – 262 (1992).

[181]	G.E.Sliter. Assessment of empirical concrete impact formulas. Proc. ASCE 106 ST5, 1023 – 1045 (1980).

[182]	V.K.Luk and M.J.Forrestal. Penetration into semi-infinite reinforced-concrete targets with spherical and ogival nosed projectiles. Int. J. Impact Engng 6, 291 – 301 (1987).

[183]	M.J.Forrestal, V.K.Luk, H.A.Watts. Penetration of reinforced-concrete with ogive-nosed penetrators. Int. J. Soilds Struct. 24, 77- 88 (1988).

[184]	R.P.Kennedy. A review of the procedures for the analysis and design of concrete structures to resist missile impact elects. Nuc. Engng and Design 37, 183 – 203 (1976).

[185]	S.H.Perry, I.C.Brown and G.Dinic. In Structural Impact and Crashworthiness, Vol. 2, pp. 617 – 627 (Edited by J. Morton). Elsevier Applied Science (1984).

[186]	S.H.Perry and J.M.Holmyard. Assessment of materials for repair of damaged concrete underwater. Imperial College of Science, Technology & Medicine Report, 0TH 90 318. HMSO (1990).

[l87]	K.G.Kufour and S.H.Perry. In Structural Impact and Crashworthiness, Vol. 2, pp. 675 – 686 (Edited by J. Morton). Elsevier Applied Science (1984).

[188]	P.Barr, P.G.Carter, W.D.Howe, A.J.Neilson and A.E.Richards. Studies of missile impact with reinforced concrete structures. Nuclear Energy 19, 179 – 189 (1980).

[189]	P.Barr. Studies of the effects of missile impacts on structures. Atom 318, 66 – 70 (1983).

[190]	P.Barr, P.G.Carter, W.D.Howe, A.J.Neilson and A.E.Richards. Experimental studies of the impact resistance of steel-faced concrete composites. 7th S. M. I. R. T. Conf., Paper JS/4 (1983).

[191]	K.Fullard, M.R.Baum and P.Barr. The assessment of impact on nuclear power plant structures in the UK. Nuc. Ending and Design 130, 113 – 120 (1991).

[192]	S.J.Hanchak, M.J.Forrestal, E.R.Young, J.Q.Ehrgott. Perforation of concrete slabs with 48 MPa (7 ksi) and 140 MPa (20 ksi) unconfined compressive strengths. Int. J. Impact Engng 12, 1 – 7 (1992).

[193]	G.G.Corbett and S.R.Reid. Local loading of simply-supported steel – grout sandwich plates. Int. J. Impact Engng 13, 443 – 461 (1993).

[194]	G.G.Corbett, S.R.Reid and S.T.S.Al-Hassani. Resistance of steel – concrete sandwich tubes to penetration. Int. J. Impact Engng 9, 191 – 203 (1990).

[195]	A.D.Gandekar, A.L.Yettram and W.A.Fletcher. Sandwich panels as an efficient form of protection against dropped objects. Struct. Engr 67, 197 – 201 (1988).