(a)

(b)

1

(c)

2

1

3

2

3

Fig. 73. A dismantled (a) 5 mm filler thickness sandwich plate and (b) 40 mm filler thickness sandwich plate following impact loading; showing (1) side view of top skin, (2) side view of filler and bottom skin, and (3) plan view of grout filler. (c) Failure cone removed from 20 mm filler thickness plate struck at below its ballistic limit [193]