Fig. 2. Projectile velocity drop through a target plate as a function of initial speed [8]:

| Variant | Target material | Target thickness, mm | Projectile diameter, mm |
| --- | --- | --- | --- |
| 1 | 4130 armour steel | 6.35 | 6.35 |
| 2 | 1020 steel (large grained) | 6.35 | 6.35 |
| 3 | 2024-Ò4 aluminium | 6.35 | 6.35 |
| 4 | 2024-Ò3 aluminium | 3.13 | 6.35 |
| 5 | 1020 steel (small grained) | 1.57 | 6.35 |
| 6 | 1020 steel (small grained) | 1.57 | 9.53 |
| 7 | 2024-Ò3 aluminium | 1.27 | 6.35 |
| 8 | 2024-0 aluminium | 1.27 | 6.35 |

Fig. 3. Measured central plug thickness  as a function of impact velocity [8]:

| Variant | Target material | Target thickness, mm | Projectile diameter, mm |
| --- | --- | --- | --- |
| 1 | 4130 armour steel | 6.35 | 6.35 |
| 2 | 1020 steel (large grained) | 6.35 | 6.35 |
| 3 | 1020 steel (small grained) | 6.35 | 6.35 |
| 4 | 2024-Ò4 aluminium | 6.35 | 6.35 |
| 5 | 2024-Ò4 aluminium | 6.35 | 9.53 |
| 6 | 2024-Ò3 aluminium | 3.13 | 6.35 |
| 7 | 1020 steel (small grained) | 1.57 | 6.35 |
| 8 | 1020 steel (small grained) | 1.57 | 9.53 |
| 9 | 2024-Ò3 aluminium | 1.27 | 6.35 |
| 10 | 2024-0 aluminium | 1.27 | 6.35 |

Fig. 4. Variation of perforation velocity (solid lines) and energy (dashed lines) with projectile mass [9]

1 - 1 - 3 mm mild steel; 2 - aluminium alloy (Beynet [11]); 3 - mild steel (Zaid [10])

Fig. 5. Variation of perforation energy with projectile nose radius for 1.3 mm thick targets [9]

1 - shear failure; 2 - tensile failure

Fig. 6. Energy absorption mechanisms for plate perforation [9]

1 - cumulative error; 2 - plugging work; 3 - membrane plastic work; 4 - plastic bending; 5 - elastic deformation; 6 - mushrooming (soft projectile); 7 - mushrooming (hard projectile)

Fig. 7. Effect of clamping force on plate ballistic limit [9]

Fig. 8. Permanent plate deflections (plate 2024-0, 368 mm in diameter, 1.27 mm thick) following impact with a spherical steel projectile (12.7 mm in diameter) [15]

Fig. 9. Transient plate profiles (plate 2024-0, 368 mm in diameter, 1.27 mm thick) at various times after impact by a steel sphere (12.7 mm in diameter) [15]

1 - 37, 2 - 67, 3 - 97, 4 - 128, 5 - 189, 7 - 372, 8 - 854 s after impact, 6 - permanent profile