Fig. 24. Peak force vs angle of incidence for a cylindro-conical projectile striking 3.18 mm thick (1) and 4.76 mm thick (2) 2024-0 aluminium targets [38]

Curves - calculated from equation (6); symbols - experimental data

Fig. 25. Results of impact tests on mild steel tubes

a - tubes with wall thickness h0=1.2 mm; b - tubes with wall thickness h0=2.0 mm;

¡ l - tubes as received ( - - - ); ¨ n - tubes as annealed ( - × - × - ) [20]