4.7. An elastic-plastic medium penetrated by a spherical particle

Consider another example of modelling the process of particle penetration into a plastic medium. The mathematical model of solid particle penetration was made by solving two boundary value problems successively. The first problem was solved for an undisturbed target with the application of the variational principle of virtual velocities and stresses. The penetration of a solid particle into a perfectly plastic medium was studied therewith. The phenomenological theory of fracture described in chapter 2 was applied, and this resulted in some corrections to the solution of the boundary value problem for a perfectly plastic medium, the corrections being entailed by a change in the mechanical properties of the target material in the region of intensive plastic flow and in the fracture zone. The second boundary value problem was solved with the use of the results obtained, and the effect of elastic waves initiated in the target by impact on the solid particle motion law was taken into account thereafter. It was assumed that, besides plastic properties (for shear strains), the target exhibits elastic compressibility. The stress tensor was determined by adding the stress deviator from the solution of the boundary value problem of perfect plasticity to the spherical tensor resulting from solving the second boundary value problem. This has offered a mathematical model of superdeep penetration of a solid particle into a disturbed elastic-plastic medium.

Assume that, on impact, a target with a height H made of a plastic material and clamped on a rigid base (fig. 40) is penetrated by a solid spherical particle of a small diameter 2R R<<H, the mass and velocity of this particle being known at some point  z=h1. Due to inertial forces, the spherical particle moves slowly in the target along the z-axis. The law of motion and the penetration depth are to be determined. Suppose that the target is made of a perfectly plastic material. At an instant of time t, the spherical particle (its mass centre) penetrates it to some depth z=h h≥R and has a velocity v. The particle remains undeformed; on the whole, its motion obeys Newton’s second law. Around the moving particle there is a region of plastic flow localised near the particle; as the particle penetrates the plastic medium, this region becomes spherical, see fig. 41. The size of the plastic flow region (radius Ro) is varied and determined from solving the corresponding variational problem.

The particle motion law needs to be defined depending on the initial value of the kinetic energy of the moving solid particle of the plastic medium.

The constitutive equations of the perfectly plastic medium and the basic functional are introduced.

Stresses in the plastic region satisfy the plasticity condition

Τ=sijsij/2=τs.

According to this condition, the intensity of tangential stresses Τ is equal to medium yield stress τs  in shear. Plastic strain rates are related to stress deviator components sij as follows:

Рис. 40. Solid particle motion in the perfectly plastic medium

ξij= H/2τssij.

The relationships introduced relate the stress to the strain one in a plastic body in the regions with discontinuous stresses and velocities. On the boundary of the plastic region moving together with the particle these parameters suffer abrupt changes; relationships for strong discontinuity waves are involved here.

z

h1

z

h1

To calculate the stress-strain state in the general boundary value problem of developed flow, we apply the technique described in section 3.6.

Let us consider the strain state of a plastic medium in the plastic flow region localised close to the moving particle and determine the boundaries of the region under study. In doing so, we suppose in the first approximation that the medium external to the intense flow region is still. The principal assumptions concerning the particle and medium motion scheme are as follows. It is supposed that the solid particle moving at a velocity vt and the plastic flow region localised around the particle are fixed to the convected spherical co-ordinate system r, ϑ, ϕ. The particle motion is treated simultaneously in the reference system (x,y,z) and in the co-ordinate system r, ϑ, ϕ. The kinematically admissible scheme of a medium under plastic strain flowing over a solid spherical particle is shown in fig. 41.

v(t)

A specific feature of the motion kinematics of the “particle – intense plastic flow region” system under deformation is that the moving (in the reference system) boundary So of the plastic flow region is the surface of the discontinuity of the tangential component of the velocity vector, i.e., the strong discontinuity surface. The normal component of the particle velocity vector in the medium under plastic strain is therewith continuous when passing the boundary So.

Рис. 41. The plastic flow region emerging around the moving particle; R0 is the radius of the plastic flow region

In the plastic flow region the medium flows all over the spherical particle. On the front surface of the particle r=R (−π/2≤ϑ≤π/2), and the tangential stresses are equal to the yield stress of the medium in shear, i.e., σrϑ=τs. On the back surface r=R (π/2≤ϑ≤3π/2), and the spalling of the medium is possible. There are no tangential stresses in this case.

The following assumptions are made for the kinematically admissible velocity field:

vϕ=0, vr≠vrϕ, vϑ≠vϑr, ϕ.

The kinematic boundary conditions

vr|r=Ro=0, vr|r=R=v cosϑ;   vr|ϑ=±π2=0, vϑ|ϑ=0, ϑ=π=0.

for the plastic flow region are matched by the following appropriate functions:

vr=v1α2−1α2R2r2−1cosϑ;   vϑ=v1α2−1sinϑ;   vϕ=0,	(245)

where α=Ro/R is a parameter to vary, which is connected with the position of the plastic zone boundary.

Note that all the further computations are made in terms of the MATLAB computer mathematics and that the references to the application of MATLAB are omitted.

The velocity field of a solid particle in the spherical co-ordinate system has the form

vr=vcosϑ;   vϑ=−vsinϑ;   vϕ=0,				(246)

Then we have the following relationships for calculating accelerations:

wr=∂vr∂t+vr∂vr∂r+vϑr∂vr∂ϑ−vϑ2r;   wϑ=∂vϑ∂t+vϑr∂vϑ∂ϑ+vrvϑr;

wϕ=0.					(247)

Formulae for the determination of the strain rate tensor components in the spherical co-ordinates in view of the assumptions made above for the appropriate functions of the velocity field assume the form

ξrr=∂vr∂r,   ξϑϑ=1r∂vϑ∂ϑ+vrr;   ξϕϕ=vrr+vϑrctgϑ;

ξrϑ=121r∂vr∂ϑ−vϑr,    ξrϕ=ξϑϕ=0.

Computations give

ξrr=−2v fr, α cosϑ, ξϑϑ=ξϕϕ=v fr, α cosϑ, ξrϕ=ξϑϕ=0,

ξrϑ=−12v fr,α sinϑ,   where   fr,α=α2α2−1R2r3.	(248)

The intensity of shear strain rate is calculated as

Η=ξrr−ξϑϑ2+ξϑϑ−ξϕϕ2+ξϕϕ−ξrr22/3+4ξrϑ2+ξϑϕ2+ξϕr2.

.

For the velocity field selected,

ξϑϑ=ξϕϕ=−ξrr/2, ξrϕ=ξϑϕ=0.

Then

Η=2 3 ξϑϑ2+ξrϑ2=v fr,α 12 cos2ϑ+sin2ϑ≈23 v fr,α cosϑ.

In order to reveal the peculiarities of the relationship between Η and the particle co-ordinates in the plastic flow region, Η was visualised. The visualization of the dependence Η=Ηr,ϑ in the reference system has shown that particles with the co-ordinates r=R , when ϑ=0 and ϑ=π, have the maximal Η.

The amount of shear strain for the particles of the medium under deformation in the region of intensive plastic flow is calculated as

Λr=totΗ dt=RorΗvr dr=23Rorr2R2−1−1drr.

The particle motion paths in the region of intensive plastic flow are determined as

rϑ,ϑoRo=1α2+sin2ϑosin2ϑ1−1α2  ϑ0<ϑ≤π−2 ϑ0 и −π−2 ϑ0≤ϑ<−ϑ0 .   ϑo<ϑ≤π−2ϑo and −π−2ϑo≤ϑ<−ϑo.

Integration gives the following result:

Λrr,ϑ=3lnα2−Ro2r2α2−1,3lnα2−Ro2r|ϑ=π22α2−1+lnrm2r2⋅r2−r2r|ϑ=π22−R2, whenwhen ϑ≤±π2;π2<ϑ<3π2..  (249)

It is necessary that shear strain acquired by the material particles of the medium when passing through the velocity jump surface So should be added to Λr,

Λϑo=vϑvcosϑo|r=Ro=1α2−1tgϑo, −π2≤ϑoπ2.

In view of the above-discussed peculiarities of the kinematically admissible velocity field, neglecting the distributed mass forces, we have the following functional of the principle of virtual velocities and stresses to solve the variational problem:

J=ΩoτsΗ'dΩ+Ωoρowivi'dΩ+Ω1ρ1wivi'dΩ+SoτsΔv'θ|r=RodSo+S1τsΔv'θ|r=RdS==i=15Ii,   (250)

where

Δv'θ|r=Ro= vtR2Ro2−R2sinθ=vt1α2−1sinϑ;   Δv'θ|r=R= vtRo2Ro2−R2sinθ=vtα2α2−1sinθ;

Δvϑ is a jump of the tangential component of the velocity vector on the surfaces So and S separating the plastic flow region and the solid spherical particle; Ωo and Ω1 are the volumes of the plastic flow region and the solid spherical particle.

- Recall that the acceleration components in Eq. (250) are not varied. In order to exclude the indefiniteness in the calculation of the integral I2, in accordance with the kinematically admissible velocity field assumed, the acceleration components are represented in the form of the following functions:

wr=f1α, Rrcosϑdvdt;    wϑ=f2αsinϑdvdt;    wϕ=0.

Here, as distinct from α=Ro/R, α=R/R, is not a parameter to be varied. It is assumed that α characterises the position of the actual boundary of the plastic flow region.

- After computing the integrals

I1=02π0πRRoτsH r2drsinθ dθ dϕ;  I2=ρo02π0πRRowivir2drsinϑ dϑ dϕ;   J3=ρ102π0πRR0wivir2drsinϑ dϑ dϕ;

I4=02π0πτsvθ|ρ=RoRo2sinθ dθ dϕ;   ,

I5=02π0πτsvθ|ρ=RR2sinθ dθ dϕ

- involved in Eq. (250), the functional J is represented as a nondimensional function of the varied parameter α, namely,

- J=α2α2−14lnα+23π−α2α2−11−1α2+1α21−1α2qot−q1t (251)

- where

- qo=−433ρoτsRdvdt≥0;   q1=−433ρ1τsRdvdt>0.

- When the densities of the medium under deformation ρo and the particle ρ1 are the same, q1=qo=q.

The functional J must assume the minimal value when α is varied. In this case, the condition

∂J/∂α=0						(252)

is fulfilled. It follows from the theorems discussed in chapter 3 that

Jα=infqdv/dt≥0Jα≈0.					(253)

on the state close to actual. It is also known that in the actual state

α=α.

Thus, we have three equations to determine three unknown quantities involved in Eq. (251).

The set of equations obtained is solved by the method of successive approximations with the use of the iteration procedure.

Having determined α=R/R and q=q|α=αwe apply the equation

q=−433ρ1τsRdvdt,

which offers a relationship to calculate the acceleration of a solid particle, namely,

wt=d2zdt2=−334qτsρ1R.						(254)

Having solved Eq. (254) with the initial conditions z|t=0=v1, z|t=0=zo, we calculate particle displacement to complete arrest as

uz=zm−zo=12v12Q,   Q=334qτsρ1R.			(255)

As a test problem, we determine the way travelled by a solid particle R=1⋅10−3m , with the initial velocity v1= 2000 m/s, in a medium with yield stress in shear τs=300 MPa on condition that ρ1=ρo=7800  kg/m3. The computations give uz=7.49⋅10−3m. Thus, the particle under study travels the distance of about 7.49 of its radius until it stops completely.

Phase trajectories of a spherical particle moving in a plastic material are constructed. For this purpose, the phase co-ordinates z1=zR, z2=z1 are introduced, then Eq. (255) is represented as a set of two differential equations,

z1=z2,   z2=−3345.3τsρ1.                                                 (256)

Fig. 42. Phase trajectories of a solid particle implanted into the target

with the initial conditions z|t=0=0, z|t=0=vo. The set is solved for particle velocities varying within the range vo=0...3000 m/s. The phase trajectories are shown in fig. 42. The path travelled by the particle is seen to be essentially dependent on the initial velocity.

Plastic deformation is generally accompanied by damage accumulated in the medium being deformed. This may reduce the resistance of the medium to particle motion considerably and increase the particle motion path. Therefore, according to the phenomenological theory of fracture, it is reasonable to determine material damage accumulation in the plastic flow region, which is associated with particle motion. To make the phenomenological theory of fracture applicable, we introduce the statically admissible stress field.

As the solid particle moves, the medium volume remains unchanged in the plastic zone, ξ=0. Consequently, the stress deviator components can be represented as

sij=σij−σ=2τsξijp/Η.

Then, for the stress tensor,

σij=σ+2τsξijp/Η.

The relationships in Eq. (256) acquire a simple form and a clear physical meaning after the intensity of shear strain rate is replaced by a close approximation,

Η≈23vtfr,αcosϑ.

Then, for the stress tensor, we have

σrr=σ−23τssgncosϑ ;     σϑϑ=σϕϕ=σ+13τssgncosϑ; σrϑ=σϑϕ=σϕr=0. (257)

Fig. 43. External forces acting on the particle

In compliance with the nature of the external loads acting on the spherical part (fig. 43), the mean normal stress σ associated with the plastic flow of the medium is presented as

σp=σ|ϑ=0cosϑ.	(258)

The stress field is statically admissible. It satisfies the equations of motion and the plasticity condition Τ=τs . The parameter σ|ϑ=0 , which remains to be determined, enables the boundary conditions to be satisfied in the integral form. To determine the parameter σ|ϑ=0, we project the stresses acting on the surface r=R of the spherical particle onto the z-axis. After the integration over the particle surface,

σ|ϑ=0=3τs34π−1−34q .				(259)

Thus, the stress-strain state of the plastic flow region is determined. Table 3 exemplifies some values of the stress state index  k=σ/τs in different zones of the plastic flow region for the test problem solved above.

Table 3

Values of the stress state index σ/τs in the plastic flow region calculated at different values of the angular co-ordinate ϑ

| ϑ | 0 | ±π/4 | ±π/2 | ±3π/4 | π |
| --- | --- | --- | --- | --- | --- |
| σ/τs | - 6.3 | - 4.4 | 0 | + 4.4 | + 6.3 |

Strain intensity is high in the plastic flow region R≤r≤Ro (fig. 41). The most intensive accumulation of damage ψ is possible here. When solving the boundary value problem of mechanics, we use the following condition: when the mean normal stresses σ take positive values (tensile stresses) in some region of a medium under deformation and ψ reaches one there, the shear yield stress of the medium becomes zero in this region, i. e. the following condition is fulfilled:

τs=τs⋅U,   where   U=1,when0,when 0≤ψ<1andψ=1and σ≤0;0<σ.    (260)

After the introduction of the unit indicator function U according to Eq. (260), the quantity τs involved in Eq. (260) is replaced by the quantity τs.

The amount of strain accumulated by the material particles of the medium moving in the plastic zone is determined according to Eq. (249).

The mathematical model is complemented by the diagram of plasticity the target material Λp=ΛpΘ,k1,k2.

The analysis of Eq. (249) has shown that Λ→∞ when r→R, consequently, a zone rich in target material continuity defects is bound to appear around the moving particle. The zone boundaries are determined from the condition Λr,ϕ,ϑ=Λpk1r,ϕ,ϑ,k2r,ϕ,ϑ. The general view of the fracture zone boundary is shown in fig. 44.

Consider now the stress-strain state of the elastic medium surrounding the plastic flow region. (It is assumed here that the plastic flow region is too small to have any tangible effect on the results of solving the elastic problem.) We suppose that the disturbance of the elastic-plastic medium preceding solid particle penetration is associated with the propagation of elastic waves in it. The target parameters are selected so that, under conditions of free vibrations, a standing wave with an invariant phase is generated in the target, the amplitude being time-variant.

In the x,y,z reference system, for a plane standing wave, the displacements of material particles can be determined as

ux=uy=0, uz=0,

uz,t=−n=1∞ancos2n+12hoπ z⋅cos 2πγnt.

They satisfy the wave equation

∂2u∂t2=c2∂2u∂x2;   c=E1−ν1+ν1−2νρo

and the boundary conditions

u|z=ho=0, u|t=0=−n=1∞ancos2n+12πzho, ∂u∂t|t=0=0

where с is the plane elastic wave propagation speed, E is the elastic modulus, ν is the Poisson ratio, γn denotes the eigenfrequencies of the plate vibrations.

The strain tensor components have the form

εzze=∂u∂t, εxxe=εyye;   εxye=εyze=εzxe=0.

The elastic stress tensor components are defined as

σzz=λ+2μεzze, σxx=σyy=λεzze.				(261)

Proceeding from Eq. (261), the mean normal stress associated with the elastic vibrations of the medium are defined as

Fig. 44. Fracture zone formation

σe=λ+23μ∂u∂t.							(262)

The sum of stresses calculated by Eqs (259) and (262) is taken as a design value of the mean normal stress in the plastic flow region. Eventually, to calculate mean normal stresses in the plastic region, we have

σ=σe+σp.						(263)

On the basis of the results obtained, an algorithm for solving the problem on the definition of the law of motion of a solid particle after penetration into a target with an elastic wave first generated in it has been developed. According to the algorithm proposed, with the use of Eqs (251) and (253), the size of the plastic flow zone (parameter Ro/R) is determined from solving the variational problem. Then the position of the fracture zone boundary lying in the region of intensive plastic flow of the target material is determined. The variational problem is again solved with the use of Eq. (260), the parameter Ro=αR being thereafter taken as the actual boundary r=Ro of the plastic flow region. The parameter q involved in the differential equation (254) is determined with the use of Eqs (252) and (253). The repeated application of Eqs (255) to (257) and Eqs (259) to (263) enables the stresses prevailing on the boundaries r=R and r=Ro to be determined completely and integrated over the surfaces, and allows the external forces affecting the spherical particle under study to be projected onto the z-axis of the reference system.

After all the forces acting on the moving solid spherical particle have been determined, Eq. (255) is amended to become

d2zdt2=−334qτsρ1R+fet					(264)

where fet is a function allowing for the influence of the shock wave on the law of particle motion.

The final step in simulating the penetration of a solid particle into an elastic-plastic medium is to integrate the differential equation (264).

For the computer simulation of the process of superdeep penetration of a solid particle into an elastic-plastic target, an imitation model, fairly simple for numerical realization, was constructed according to the algorithm described. The method of object-oriented visual programming was applied. The programming was effected in the Visual Studio environment, with the use of the MATLAB + Simulink computer mathematics system.

4.8. Thin plate perforation by a flying ball

Consider another simple problem on impact deformation and fracture, namely, thin circular plate perforation by a rigid ball.

Assume that a rigid ball of mass m and radius Rs flying at a constant velocity vs0 impinges on the centre of a thin circular plate of thickness h and radius R, fig. 45 a. The plate is clamped around the periphery. On the right of the plate there is a medium resisting the plate motion. One needs to calculate the stress-strain state and damage of the plate, to predict the instant and site fracture, and other parameters accompanying impact.

The problem will be stated and solved approximately in the convected Lagrangian co-ordinate. The Cartesian system x, y, z is selected as the Eulerian co-ordinate system. At the initial instant the Lagrangian system coincides with the cylindric co-ordinate system r, ϕ, z with the origin lying in the plate centre. For the sake of simplicity, the following assumptions are made: the plate radius far exceeds the plate thickness, which remains the same throughout the deformation, all the stress-strain parameters being invariant through the whole plate thickness. In this case, radial and axial strains are negligible at high ball velocities. The metric tensor for the Lagrangian co-ordinate system may be considered approximately equal to the metric tensor of the cylindric co-ordinate system.

Fig. 45. A chart to the problem on the deformation and fracture of a thin plate impacted by a ball flying at a velocity v0

Let us now formulate the boundary conditions. The plate is clamped around the periphery,

vi|r=R=0, i=r, ϕ, z.					(265)

On the right of the plate there is a medium exhibiting resistance to the motion of the right surface of the plate. Assume that the interaction between the plate and the medium is expressible in the form of a function relating the surface stress to the velocity of the boundary points,

fi=fi(vj), i,j=r, ϕ, z.					(266)

This dependence is assumed to have the form

fi=kvi							(267)

where k is a known coefficient.

The left surface of the plate being deformed, except the ball-plate contact area, is free from surface stresses. The concentrated force of impinging ball action operates in the plate centre.

Let us consider that the plate material is isotropic, that the stress deviators and strain rate deviators are similar. Suppose also that this material is incompressible, rigid-plastic, and that it suffers developed plastic deformations, so that elastic deformations can be neglected. These suppositions are matched by the following constitutive equations for the deviatoric part:

sij=2ΤΗeij,   Τ=τs+μΗ					(268)

where μ is viscosity, a known material constant.

To simplify the problem, we resort to the assumption that the plate perforated by a rigid ball is very thin. In this connection the stressing on the right surface of the plate, which is predetermined by the resistance of the medium, may qualify as mass force,

ρgz=fz=kvz, gr=gϕ=0,					(269)

And this makes the problem one-dimensional.

Let us make some other assumptions simplifying the problem solution. Assume that, starting from the instant t0 (see fig. 45), which is the instant of the process onset, there is sticking of some part of the ball surface to the plate surface. The sticking part is assumed to be rigid.

Let us solve the problem stated in the previous section by the method presented in section 3.6. For the problem under study, the functional of the principle of virtual velocities and stresses has the form

J=2 π h RrRτs Η'+μ Η'22+Τ'22μ−τs Τ'μ+ρ wi−k vi vi'rdr−F vz'|r=0		(270)

where Rr is the radius of the rigid sticking zone; F=−mwz|r=0 – ball action force.

At an arbitrary instant we seek an extremum on the following class of virtual states. The virtual velocity field is selected as

vr'=0, vϕ'=0, vz'=v exp−a r2					(271)

where v, a are the parameters to be varied at each instance, or, in general terms, the time functions to be found. Assuming this form of the virtual velocity field, we satisfy the condition of peripheral plate clamping approximately; however, it will be shown in what follows that the error of this approximation can be made as small as is wished due to the initial conditions selected. The preanalysis has shown that, with the parameters assumed in this section, the ball radius Rr=Rs can be taken as the sticking zone radius for the virtual field expressed by Eq. (271).

The only zero component of the strain rate tensor is

ξrz'=−avrexp−ar2.						(272)

Then the shear strain rate intensity becomes

Η'=2avrexp−ar2.						(273)

Turn to the virtual stress field. As the radial and axial strains are considered to be negligible, σrz is assumed to be the only zero component of the stress tensor. Then the virtual value of σrz' must satisfy the motion equation

∂σrz'∂ r+σrz' r=ρwz−kvz 					(274)

where wz, vz are the actual values of acceleration and velocity. Integrating Eq. (274), we arrive at

σrz'=1r ρ wz−k vz dr+c				(275)

where c is another quantity to be varied, a time function. In terms of the assumptions made, the intensity of tangential stresses becomes

Τ'=σrz'.							(276)

Thus, at an arbitrary instant, we have three parameters to be varied, v, a, c, which determine the virtual state. As in the preceding section, the extremum of the functional at a fixed point in time is sought by the Ritz method. When the necessary conditions of the extremum of the functional (270),

∂J∂v=0, ∂J∂a=0, ∂J∂c=0,						(277)

after differentiating with respect to the parameters v, a, c, have the value of acceleration

wz=dvdt−v r2dadt exp−a r2					(278)

substituted in them, we arrive at the following set of equations:

−dvdt v ρ RsRr3 exp−2 a r2 dr+v2 RsR4 n a r3 1−a r2−k r3 exp−2 a r2 dr−

−dadt v2 ρ RsRr5 exp−2 a r2 dr+2 a τs RsRr2 1−a r2 exp−a r2 v dr=0,	(279)

2 π h (dvdt ρ RsRr exp−2 a r2 dr+v RsR4 n a2 r3−k r exp−2 a r2 dr−

−dadt v ρ RsRr3 exp−2 a r2 dr+2 a τs RsRr2 exp−a r2 dr)+dvdt m=0,	(280)

c=τs−1lnR−lnRs RsR1r ρ dvdt−v r2dadt−k v exp−a r2 r dr dr.  (281)

Equations (279) and (280) make a set of two ordinary differential first-order equations with respect to the functions v=v(t) and a=a(t). Solving this set, one determines the strain state of the plate on the time interval between t=t0 to the instant of fracture. Equation (281) is algebraic. It enables one to find the values of c=c(t) at each instant t from the known v=v(t) and a=a(t) and, in view of Eq. (275), to determine the stress state over the whole period of deformation to rupture.

Turn now to the specification of the initial conditions v0=v(t0) and a0=a(t0) required to solve the differential equations. The point in time at which the ball crosses the plane z=0 completely is taken as the initial instant, see fig. 45 b. Consider that the whole momentum of the ball mvs0 has by this time t0 been transferred to the ball–plate system, and that the ball thereafter moves together with the plate up to the instant of fracture. It follows from the condition of momentum conservation that

mvs0=m v0+2 π h Rs ρ v0+2 π h ρ v0 RsRexp−a0 r2 r dr.		(282)

One more equation is required to determine v0 and a0. The condition of small but known displacement of the plate boundary by the instant t0 can be taken as an equation to serve this purpose. In other words, the fulfillment of the plate clamping condition is presumed to be approximate with a given error. According to the presumption, by the time t0, the plate centre will have displaced from the initial position by the value 2Rs, fig. 45 b. In this case, the plate points with the co-ordinate r=R will have displaced along the z-axis by the value 2Rsexp−a0R2. Suppose that this excursion must not exceed 0.01h. This condition enables the condition of plate clamping in the course of deformation to be fulfilled with an error not exceeding the plate thickness h. The presumption offers the required parameter as

Fig. 46. The instant of plate fracture tf as dependent on the initial velocity of the ball vs0.

a0=1R2ln200Rsh.							(283)

The value of v0 is determined from Eq. (282) by the value of a0 obtained.

Thus, we have the set of equations and the initial conditions enabling the stress-strain state to be calculated.

In parallel with solving the set of equations (279) to (281), one can predict material damage at point of the plate. For the stress state selected, its indices introduced in section 1.1 are constant at each point of the plate, at any instant of deformation, and they have the following values: k1=σΤ=0, k2=μσ=1. As the deformation of each particle is monotonic, damage can be determined from solving the differential equation

dψdt=ΗΛp. 						(284)

In view of the fact that ψ(t0)=0, the value of damage is

ψ(t)=ΛΛp.						(285)

Fig. 47. Ball velocity at the instant of fracture,

vf, as dependent on the initial velocity vs0

The solution of the set of equations (279) to (281) and the prediction of damage are effected up to the instant of plate fracture.

Calculations were made for the following parameters of the process of steel ball impact on a steel plate: τs=200MPa, R=0.1m, Rs=0.005m, h=5⋅10−4m, ρ=7800kgm3, μ=0.2Pa⋅s, Λp=0.2, k=−104kgm2s, vs0=700 − 1500ms.

For the parameters assumed, at the initial ball velocity vs0 lower than 700ms, no plate perforation occurs. The calculation results are presented in figs 46 to 49. In all the cases, fracture occurs around the circumference r=Rs. Figure 46 shows the instant of fracture as dependent on the ball velocity. The pre-fracture time decreases as the impact velocity increases. Figure 47 shows ball velocity at the instant of fracture t=tf as dependent on the initial ball velocity. Increasing metal damage at the site of future rupture for the initial ball velocity 1000ms is shown in Fig. 48. Figure 49 shows predicted values of the departure of the plate boundary from the initial position that has occurred by the instant of fracture. In other words, the error in the fulfillment of the boundary clamping condition is demonstrated. It is obvious from the figure that the error is two orders of magnitude less than the plate thickness.

4.9. A plane solution to the plate perforation problem

In the previous section, in solving the problem on plate perforation by a ball, the boundary conditions expressed by Eqs (266) and (267) were treated as an equation for mass forces. In this section the principle of virtual velocities and stresses is formulated in view of these boundary conditions, and this enables the same problem to be solved in terms of the plane statement.

Consider the following boundary value problem of the theory of plastic flow. To find: the values of the velocity vector and stress tensor components at some point in time at each point of the body V under deformation that would satisfy the equations of motion (116), the kinematic equations (115), the constitutive equations (124) and the boundary conditions. Assume that the boundary conditions are as in Eq. (86 a), and that on some part of the surface the following conditions are specified:

Fig. 48. Accumulation of material damage ψ at the site of the future rupture.

∀M∈Svf fi=fivj.		(286)

As before, the functions given by Eqs (124) and (286) are set to be soluble in the general case with respect to eij, ξ and vi respectively and satisfying the necessary conditions of the existence of the problem solution. Particularly, ∂ σ∂ ξ>0, ∂ sij∂ ekl|i=kj=l>0, ∂ fi∂ vj|i=j>0.

- Fig. 49. The error in the fulfillment of the plate clamping condition, Δ, at the instant of fracture

The boundary value problem is in this case equivalent to the variational equation

δJ=δV0eij'sijekl deij+0sij'eijskl dsij+0ξ'σξ dξ+0σ'ξσ dσ+ρ wi−gi vi' dV−

,			(287)

which represents the principle of virtual velocities and stresses for the instance of the boundary conditions as in Eq. (286). All the basic theorems of the principle will assert. The friction law represented by Eq. (86 b) can be viewed as a particular case of the boundary conditions written by Eq. (286). In this case, the variational principle presented in Eq. (287) takes the known form of Eqs (117), (118) and (131).

Consider now solving the problem described in section 4.7 with the application of the variational principle (287). Thus, we take into consideration the boundary conditions written by Eqs (266) and (267) explicitly, through solving a plane problem. We consider that the parameters of the stress-strain state depend on the co-ordinate z. All the other assumptions hold true. The functional (287) becomes

J=2π (0hRsRτs Η'+μ Η'22+Τ'22 μ−τs Τ'μ+ρ wz z' r dr dz−

−RsRk vz'22+σzz'22 k|z=hr dr)−F vz'|z=0r=0				(288)

where F is the concentrated force exerted on the plate by the ball.

We set the virtual velocity field as

vr'=0, vϕ'=0, vz'=v+b z exp−a r2,				(289)

where v, a, b are parameters to be varied at each instant, or, in general terms, the required time functions. Two strain rate tensor components are nonzero,

ξzz'=b exp−a r2,   ξrz'=−a r v+b z exp−a r2.		(290)

The incompressibility condition is not fulfilled In this case. However, the volumetric strain is considered to be insignificant, and it is not taken into account in Eq. (288).

The intensity of shear strain rates becomes

Η'=4 ξrz'2+43 ξzz'2.					(291)

The virtual field is assumed to be also determined by two nonzero stress tensor components – σzz' and σrz'. Assume that σzz' has the form

σzz'=c1 z exp−a r2.						(292)

This enables the boundary condition on the load-free surface z=0 to be fulfilled. In terms of the assumptions made, the equations of motion have the form

∂σrz'∂z=0,

∂ σzz'∂ z+∂ σrz'∂ r+σrz'r=ρ wz						   (293)

where wz is the actual value of acceleration. By integrating the second equation of motion (293) with respect to σrz', we obtain

σrz'=1r ρ wz−∂ σzz∂ z r dr+C				(294)

where C is an arbitrary function independent of r. We determine it from the first equation (293) as

C=ρ z2 a d bd t−d ad t r−1a exp−a r2+c2.			(295)

In Eqs (292) and (295) c1 and c2 are quantities to be varied, functions of time. The intensity of tangential stresses is represented as

Τ'=29 σzz'2+σrz'2.						(296)

Thus, at an arbitrary point in time, we have five parameters to be varied – v, a, b, c1 and c2 determining the virtual stress-strain state of the plate. As before, the functional extremum at a fixed instant is determined by the Ritz method. Substituting into the necessary extremum conditions of the functional (288)

∂J∂v=0, ∂J∂a=0, ∂J∂b=0, ∂J∂c1=0 , ∂J∂c2=0,			(297)

after differentiation, the values of acceleration

wz=d v∂ t+d b∂ t z−v+b z r2 d a∂ t exp−a r2			(298)

And concentrated force

F=−m wz|r=0z=0,	(299)

we arrive at a set of two groups of equations,

Fig. 50. Plane solution. The instant of plate rupture tf as dependent on the initial ball velocity vs0.

F1v, a, b, dvdt, dadt, dbdt=0,

F2v, a, b, c1, c2=0.	(300)

The first group is a set of three linear ordinary differential equations with respect to the functions vt, at, bt. As the initial conditions necessary for solving the set, we take the values v0=v(t0) and a0=a(t0) found from Eqs (282) and (283) and the value b0=b(t0)=0 ensuing from the assumption that the plate begins to deform at the instant t=t0.

Fig. 51. Plane solution. Ball velocity at the instant of fracture vf as dependent on the initial velocity vs0

The second group consists of two algebraic equations determining the values of the parameters c1 and c2 at an arbitrary instant t by the values of v, a and b found. Thus, the set of equations obtained allows a change in the stress-strain state of the plate prior to fracture to be determined.

In parallel with the determination of the stress-strain state, one can predict material damage at each point of the plate. The value of damage, as in section 3.1, is found from Eq. (285), the function (183) used in section 4.1 being taken as Λp, with the following values of the parameters: χ=0.2, λ=−2.

The stress-strain state and damage of the material were calculated with the same process parameters as in section 4.7. The calculation results are presented in figs 50 to 53. Figure 50 shows the value of the instant of fracture as dependent on ball velocity. Figure 51 depicts ball velocity at the instant of fracture t=tf as dependent on the initial ball velocity. Compared with figs 46 and 47, these dependences show that the ultimate value of damage is reached sooner in plane calculations. The comparison between the error shown in fig. 52 and that shown in fig. 49 demonstrates that the error in the fulfilment of the plate clamping condition is lower in the plane solution.

Fig. 52. Plane solution. The error in the fulfillment the plate clamping condition Δat the instant of rupture

The study of the calculation results shows that the one-dimensional solution fails to offer a qualitative estimation of the effect the properties of the medium adjacent to the plate exert on deformation and fracture. The plane solution offers this estimation. Figure 53 shows plate centre displacement with time prior to fracture at the initial ball velocity 1000ms for different values of the coefficient k in Eq. (267). The analysis of the results testifies that, as the absolute value of the coefficient grows, the duration of deformation to before fracture increases, whereas the plate deflection and ball velocity at the instant of fracture decrease.

The calculations suggest that the variational principle of virtual velocities and stresses represented by Eq. (287) enables one to solve problems with boundary conditions like in Eq. (286). The solution made with the application of this principle seems to be more adequate than the one-dimensional one.

Fig. 53. Plane solution. The motion of the plate centre

prior to rupture: 1 – one-dimensional solution,

k=−103÷−105kgm2s, 2 – k=−103kgm2s,

3 – k=−104kgm2s, 4 – k=−105kgm2s.

REFERENCES TO PART II

1.	Седов Л.И. Механика сплошной среды. Т.1, 492 с., Т. 2, 568 с. М.: Наука, 1970.

2.	Ильюшин А.А. Механика сплошной среды. М.: Изд-во МГУ, 1978. 286 с.

3.	Колмогоров В.Л. Напряжения, деформации, разрушение. М.: Металлургия, 1970. 230 с.

4.	Колмогоров В.Л., Богатов А.А., Мигачев Б.А. и др. Пластичность и разрушение. М: Металлургия, 1977. 365 с.

5.	Паршин В.А., Зудов Е.Г., Колмогоров В.Л. Деформируемость и качество. М.: Металлургия, 1979. 192 с

6.	Мигачев Б.А., Потапов А.И. Пластичность инструментальных сталей и сплавов. Справочник. М.: Металлургия, 1980. 89 с.

7.	Богатов А.А., Мижирицкий О.И., Смирнов С.В. Ресурс пластичности металлов при обработке давлением. М.: Металлургия, 1984. 150 с

8.	Унксов Е.П., Джонсон У., Колмогоров В.Л. и др. Теория пластических деформаций металлов / Под ред. Е.П. Унксова, А.Г .Овчинникова. М.: Машиностроение, 1983. 598 с

9.	Колмогоров В.Л. Механика обработки металлов давлением. М.: Металлургия, 1986. 688 с.

10.	Унксов Е.П., Джонсон У., Колмогоров В.Л. и др. Теория ковки и штамповки / Под ред. Е.П. Унксова, А.Г. Овчинникова.- Изд. 2-е, переработ. и доп. М.: Машиностроение, 1992. 720 с.

11.	Kolmogorov, V.L. Model of metal fracture in cold deformation and ductility restoration by annealing // Materials Processing Defects./ Eds. S.K.Ghosh and M.Predeleanu, Elsevier Science B.V. 1995, p. 219

12.	Burdukovsky, V.G., Kolmogorov, V.L., Migachev, B.A. Prediction of resources of materials of machine and construction elements in the process of manufacture and exploitation. // Journal of Materials Processing Technology, 1995. V. 55. p. 292-295.

13.	Kolmogorov, V.L. Friction and wear model for a heavily loaded sliding pair. Part I. Metal damage and fracture model. // Wear, 1996.V. 194, p. 71-79.

14.	Kolmogorov, V.L., Smirnov, S.V. Healing of metal microdefects after cold deformation. // Advanced Methods in Materials Processing Defects. Eds. M.Predeleanu and P.Gilormini , 1997. Elsevier. p. 61.

15.	Владимиров В.И. Физическая природа разрушения металлов. М.: Металлургия, 1984. 280 с.

16.	Качанов Л.М. Основы механики разрушения. М.: Наука, 1974. 311 с.

17.	Работнов Ю.Н. Механика деформируемого твердого тела. М.: Наука, 1979. 744 с.

18.	Болотин В.В. Прогнозирование ресурса машин и конструкций. М.: Машиностроение, 1984. 312 с

19.	Богатов А.А., Смирнов С.В., Быков В.Н. и др. Авт. свид. SU N1422090 А1, Бюллетень изобретений и открытий, N33 (1988).

20.	Богатов А.А., Смирнов С.В., Быков В.Н. и др. Обработка металлов давлением: Межвузовский сборник. Свердловск: Изд. УПИ, 1991. с. 45.

21.	Karman, T. Mitteilung Forschungsarbeit Vereinigte Deutsche Ingenier, 118, Berlin, 1913.

22.	Bridgman, P.W. Studies in large plastic flow and fracture, McGraw-Hill, N.Y., 1952. 444 p.

23.	Mechanical behaviour of materials under pressure. / Ed. by H.Ll.D. Pugh. Elsevier Publishing Company, 1970. 292 p.

24.	Давиденков Н.Н., Спиридонова Н.И. Анализ напряженного состояния в шейке растянутого образца. // Заводская лаборатория, 1945. Т. XI, N 6, с. 583-593.

25.	Разрушение. Т. 3 / Под ред. Г. Либовица. М., Машиностроение, 1977. 796 с.

26.	Смирнов С.В., Шохин В.А., Колмогоров С.В. Оценка деформируемости при правке рельсов на роликоправильных машинах // Обработка металлов давлением: Межвузовский сборник научных трудов. Свердловск: УПИ, 1987. с. 64-74.

27.	Кийко И.А .// Обработка металлов давлением. Вып.9. Межвузовский сборник. Свердловск, Изд.УПИ, 1982, с.27-40.

28.	Колмогоров В.Л., Мигачев Б.А. Прогнозирование разрушения металлов в процессе горячей пластической деформациию // Изв. АН СССР. Металлы, 1991. N 3, 124c.

29.	Губкин С.И. Пластическая деформация металлов. Т.II. Физико-химическая теория пластичности. М.: Металлургиздат, 1960. 416 с.

30.	Чурбаев Р.В., Добромыслов А.В., Колмогоров В.Л. и др. Влияние скорости деформации на пластичность металлов под давлением. ..Физика металлов и металловедение, 1990. N 6, c. 178 - 183.

31.	Speedy, N.B., Brown, R.F., Goodwin, G.C. Control theory: identification and optimal control. Edinburgh: Oliver and Bound, 1970.

32.	Справочник по теории автоматического управления / Под ред. А.А.Красовского. М.: Наука, 1987. 711 с.

33.	Коновалов А.В. Построение динамических моделей сопротивления металлов пластической деформации методами теории идентификации. Изв. АН СССР. Металлы, 1984. N 6, c. 178-180.

34.	Коновалов А.В., Селиванов Г.С., Антошечкин Б.М. О динамической модели сопротивления металла пластической деформации. // Изв. АН СССР. Металлы, 1987..N. 4, с. 122-127.

35.	Богатов А.А., Смирнов С.В., Зеленский В.Н. и др. Использование диаграмм пластичности для выбора термической обработки перед деформацией. // Сталь, 1984. N 2, с. 69 - 71.

36.	Белов В.А., Богатов А.А., Головин В.А. и др. Исследование изменения поврежденности стали 40Х при холодной пластической деформации и термической обработке. // Физика металлов и металловедение, 1985, Т. 54, V. 4, с. 787 - 792.

37.	Богатов А.А., Тропотов А.В., Власов В.М. и др. Электросварные холоднодеформированные трубы. М.: Металлургия, 1991. 207 с.

38.	Богатов А.А., Смирнов С.В., Михайлов В.Г. и др. Технологические свойства сплавов системы W-Ni-Fe при обработке давлением. // Кузнечно-штамповочное производство, 1991. N. 6, с. 8-10.

39.	Смирнов С.В., Швейкин В.П., Михайлов В.Г. и др. Сравнительное исследование пластичности прутков из вольфрамового сплава ВА после ротационной ковки и прокатки. // Кузнечно-штамповочное производство, 1994.N. 8, c. 2-4.

40.	Мигачев Б.А., Потапов А.И. Пластичность инструментальных сталей и сплавов. М.: Металлургия, 1980. 89 с.

41.	Потапов А.И., Мигачев Б.А. Совершенствование режимов нагрева кузнечных слитков с целью улучшения их деформируемости. // Кузнечно-штамповочное производство, 1983. N. 6, с. 34-37.

42.	Мигачев Б.А., Тунева Л.Д. Влияние условий деформирования на качество поковок быстрорежущей стали. // Кузнечно-штамповочное производство 1987. N. 3, c. 14-15.

43.	Мигачев Б.А., Волков В.П. Влияние циклической ковки на механические свойства поковок конструкционной углеродистой и легированной стали. // Кузнечно - штамповочное производство, 1995. N. 10, с. 15-17.

44.	Мигачев Б.А., Теляшов Н.В. Возможности дефектоскопии при контроле качества горячекатаных трубных заготовок // Дефектоскопия, 1994. N. 9, c. 46-49.

45.	Мигачев Б.А., Добыш Н.М. Квалиметрия проката быстрорежущей стали в условиях заготовительного производства с кузнечным переделом //  Дефектоскопия. 1995, N 6, с.80 - 83.

46.	Manson, S.S. Thermal stress and low-cycle fatique. New York. McGraw - Hill Book Comp. 1966.

Менсон С. Температурные напряжения и малоцикловая усталость. / Пер. с англ. М.: Машиностроение, 1974.

[47]	Серенсен С.В., Шнейдерович Р.М., Гусенков А.П. др. Прочность при малоцикловом нагружении. Основы метода расчета и испытаний. М.: Наука, 1975. 285 c.

[48]	Иванова В.С., Терентьев В.Ф. Природа усталости металлов. М.: Металлургия, 1975. 456 с.

[49]	Collins, J.A. Failure of materials in mechanical design. A.Wiley - Interscience Publication John Wiley & Sons. New York, Chichester, Brisbane, Toronto, Singapore. 1981. p. 188-193.

Коллинз Дж. Повреждения материалов в конструкциях. / Пер. с англ. М.: Мир, 1984. 624 с.

[50]	Ищенко И.И., Погребняк А.Д. Прочность, долговечность и разрушение конструкционных материалов при многоцикловом нагружении (Обзор).. // Прикладная механика 1997, N 33 N 4, c. 3-27.

[51]	Головин C.А., Пушкар А. Микропластичность и усталость металлов. / Под ред. С.А.Головина. М.: Металлургия, 1980. 239 с.

[52]	Колмогоров В.Л. Принцип возможных изменений напряженного и деформированного состояний. // Механика твердого тела 1967, Т 2, с. 143-150.

[53]	Baltov, A. Variational theorems in the dynamic theory of viscoplasticity. // Bull. de l’Acad. Pol. Sci. ser. Sci. Techn. 1969. V. 17 , N 5. p. 297-304.

[54]	Колмогоров В.Л. Метод расчета напряженно-деформированного состояния в общей краевой задаче развитого течения. // Вестник ПГТУ. Механика, N 2, Пермь: Пермский государственный технический университет, 1995, с. .87-97.

[55]	Колмогоров В.Л., Спевак Л.Ф., Трухин В.Б. Метод расчета напряженно-деформированного состояния в общей краевой задаче обработки металлов давлением. // Технология легких сплавов, 1995, N 4, c. 39-49.

[56]	Гасилов В.Л., Колмогоров В.Л., Спевак Л.Ф. Модель разрушения в процессах развитого деформирования металлов: Тр. 9-й конф. по прочности и пластичности. Москва, 22-26 января 1996г.. Прочность и пластичность. Т .2, 1996.  с. 58-63.

[57]	Колмогоров В.Л. Некоторые теоретические проблемы ОМД и возможные пути их решения. // Пластическая деформация сталей и сплавов: Cб. Науч. Тр. М.,: МИСИС, 1996. с. 140-151.

[58]	Kolmogorov, V.L., Lapovok, R.E. The calculation of stress-deformed state under non-isothermicplastic flow - the example of psrallelepiped setting. // Computers and Structures,  1992, V. 44, N 1-2, p. 419-424.

[59]	Kolmogorov, V.L., Fedotov, V.P., Spevak, L.F. A mathematical model for the formation and development of defects in metals. // Advanced Methods in Materials Processing Defects. / Eds. M.Predeleanu and P.Gilormini, 1997, Elsevier. p. 51.

[60]	Хилл Р. Математическая теория пластичности. Пер. с англ. М.: Гостехиздат, 1956.. 407 c.

[61]	Федотов В.П. Вариационные решения упругопластических задач: Матер. Конф. “Актуальные проблемы пластической обработки металлов”. Варна, Болгария, 1990. с.223-227.

[62]	Полищук Е.Г. Метод граничных элементов для расчета жестко-вязко пластических течений. // Прикладная математика и механика, 1992, T. 56, N 5, c. 691-695.

[63]	Biot, M. Variational Principles in Heat Transfer. Oxford University Press, 1970.

Био, М. Вариационные принципы в теории теплообмена. М., “Энергия”, 1975. 206 с.

[64]	Айнола Л.Я. Вариационные принципы для нестационарных задач теплопроводности. // Инженерно - физический журнал, 1967, T. XII, N 4. с. 465-468.

[65]	Готлиб Б.М., Добычин И.А., Баранчиков В.М. Основы статистической теории обработки металлов давлением. М.: Металлургия, 1980. 168 с.

[66]	Johnson, W., Chandrasekar, S. Rupert’s glass drops: Residual-stress measurements and calculations and hypotheses for explaining disintegrating fracture. // Journal of Materials Processing Technology, 1992, V. 31, p. 413-440.

[67]	Колмогоров В.Л. О применениии энергетических принципов теории пластичности к решению задач обработки металлов давлением. // Тр. Уральск. Политех. Ин-та, 1958. N64.. c.

[68]	Gerhardt, J. Numerische Simulation dreidimensionaler Umformvorgange mit Einbezug des Temperaturverhaltens. Springer - Verlag, Berlin, Heidelberg, 1989, (Deutsch).

[69]	Kolmogorov, V.L., Lapovok, R.E. The calculation of stress-deformed state under non-isothermic plastic flow - the example of parallelepiped setting. Computers and structures 1992, 44 No. 1/2.

[70]	Горобцов В.Г., Ушеренко С.М., Фурс В.Я. О некоторых эффектах обработки высокоскоростной струей рабочего вещества. Порошковая металлургия. Минск, Выcшая школа, 1979, вып.3, с.8 - 12.

[71]	Веддер Дж.Ф., Майдевиль Ж.К. Механика образования воронок при ударе и взрыве. Под ред. А.Ю.Ишлинского и Г.Г.Черного, вып.12. М., 1977. с. 7-32.

[72]	Козорезов К.И., Максименко В.Н., Ушеренко С.М. Исследование эффектов взаимодействия дискретных микрочастиц с твердым телом. - В кн.: Избранные вопросы современной механики. - M.: Издательство Московского университета. 1981, с.114 - 119.

[73]	Андилевко С.К., Роман О.В., Романов Г.С. и др. Сверхглубокое проникание частиц порошка в преграду. - В кн.: Порошковая металлургия. Минск, Высшая школа, 1985, вып.9, с.3 - 13.

[74]	Роман О.В., Горобцов В.Г., Дубровская Г.Н. и др. Исследование материалов на основе железа после ударного взаимодействия с потоком порошковых частиц. АН СССР и ЭССР. Третье всесоюзное совещание по детонации, 11 - 14 ноября, Таллин, Тезисы докладов, Черноголовка, 1985, с.96.

[75]	Андилевко С.К., Сай Е.Н., Романов Г.С. и др. Перемещение ударника в металле, подвергнутом предварительно ударноволновому нагружению. Там же, с.97.

[76]	Ворошнин Л.Г., Горобцов В.Г., Шилкин В.А. Упрочнение быстрорежущей стали Р6М5 при динамическом микролегировании и термической обработке. Доклады АН БССР 1985, ХХI (1), с. 57-58.

[77]	Горобцов В.Г., Дубровская Г.Н., Ушеренко С.М. и др. Физико - химические исследования некоторых вопросов взаимодействия высокоскоростных порошковых частиц с металлической мишенью. Действие высоких давлений на материалы. Киев. Наукова думка, 1986, с.101 - 102.

[78]	Киселев Ю.Н., Миронов Э.А., Попов В.А. и др. О механизме взаимодействия потока микрочастиц с преградой. Детонация и ударные волны. Материалы VIII всесоюзного симпозиума по горению и взрыву. 13 - 17 октября 1986, Ташкент.

[79]	Шилкин В.А., Ушеренко С.М., Андилевко С.К. Введение в сталь металлических порошков. - В сб. Обработка материалов при высоких давлениях. Киев: ИПМ АН УССР, 1987, с.99 - 102.

[80]	Андилевко С.К., Сай Е.Н., Романов Г.С. и др. Перемещение ударника в металле. Физика горения и взрыва 1988, 5, с. 110-113.

[81]	Альтшулер Л.В., Андилевко С.К., Романов Г.С. и др. О модели сверхглубокого проникания. Письма в ЖТФ, 1989, 15 (5), с. 55-57.

[82]	Андилевко С.К., Романов Г.С., Ушеренко С.М. и др. Сверхглубокое проникание дискретных микрочастиц. Всесоюзное совещание по детонации. Сборник докладов, 1 том. Красноярск, 5 - 12 августа, 1991, с. 38-42.

[83]	Андилевко С.К. Сверхглубокий массоперенос дискретных микрочастиц в металлических преградах в условиях нагружения последних потоком порошка. Автореферат диссертации на соискание ученой степени кандидата физико-математических наук. Академический научный комплекс “Институт тепло- и массообмена”, Минск, 1991. 106 с.

[84]	Григорян С.С. О природе “сверхглубокого” проникания твердых микрочастиц в твердые материалы. Доклады академии наук СССР 1987, 292 (6), с. 1319-1323.

[85]	Черный Г.Г. Механизм аномально низкого сопротивления при движении тел в твердых средах. Доклады академии наук СССР 1987, 292, (6), с. 1324-1328.

[86]	Naimark, O.B. Nonlinear aspects of damage kinetics and some anomalies of deformation and failure under intense loading. Euromech 362, UMIST 21st-23rd April, 1997.

The solution was made by A.G. Zalazinsky and E.A. Zalazinskaya with the participation of V.L. Kolmogorov

The problems in sections 4.8 and 4.9 were solved by V. P. Fedotov and L. F. Spevak with the participation of the author